Bio-Parts Cleaner/Degreaser (Soy Based)

# "Biobased Lubricants that Perform Like Synthetics"

A specially formulated, ultimately biodegradable1 Soy Cleaner/Degreaser that can be used to replace petroleum solvents for cleaning parts and equipment.  This safe, nonflammable product contains no Volatile Organic Compounds (VOCs), and has been formulated with anti-oxidants for improved stability.  (Excellent electrical insulating value)

### TYPICAL TEST DATA:

ASTM D-445 3.9 cSt @ 40ºC				ASTM D-2500 Cloud Point -5.5oC

ASTM D-92 Flash Point 149 ºC				ASTM D-97 Pour Point -12oC

Pound Per Gallon   7.16					ASTM D-130 Copper Corrosion 1a

ASTM D-877 Dielectric Strength   >40KV			ASTM D-1160 Distillation Temp 355 oC

Bio-Cleaner/Degreaser (plus Corrosion Protection) (Soy Based)

A specially formulated, ultimately biodegradable1 Soy Cleaner/Degreaser that can be used to replace petroleum solvents for cleaning parts and equipment.  This safe, nonflammable product contains no Volatile Organic Compounds (VOCs), and has been formulated with anti-oxidants and corrosion inhibitors for improved stability.

### TYPICAL TEST DATA:

ASTM D-445 4.3 cSt @ 40ºC

ASTM D-92 Flash Point 149 ºC

Pound Per Gallon   7.16

Bio-General Purpose Cleaner/Degreaser

(Water Emulsifiable) (Soy Based)

An excellent biobased, ultimate biodegradable1 product that can be used to replace petroleum solvents for cleaning parts and equipment.  May be used as a straight solution or may be solubilized with water before use.  When used as a straight solution the product cleans and breaks down easily with a garden hose or pressure washers.  Provides short term corrosion protection.

### TYPICAL TEST DATA:

ASTM D-445 36 cSt @ 40ºC

ASTM D-92 Flash Point 270ºC

ASTM D-97 Pour Point -24 ºC

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

* Trademark of Renewable Lubricants, Inc.

Copyright 2002 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA	 1 Gallon      5 Gallon Pails    Drums    Bulk