### Bio-Fleet™ TC+ 2-Cycle Engine Oil

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Fleet™ TC+ 2-Cycle Engine Oil is a patented, readily biodegradable1 biobased formula with improved additive technology that meets and exceeds API TC+ for high performance air-cooled 2 Cycle Engines.  This improved additive technology provides additional antiwear/anti-scuffing protection and is recommended for used in lawn and garden equipment, chain saws, snow blowers, motor scooters, mopeds, air-cooled snowmobiles, and air-cooled marine engines.

Bio-Fleet™ TC+ contains enhanced lubricity boosters and additional cleanliness chemistry that improves lubrication performance for high output Motorcycle and Husqvarna Chain Saw 242/266 requirements.  It is specifically formulated to reduce visible smoke and burn clean, minimizing deposits and carbon buildup, and preventing ring sticking and spark plug fouling.  In addition, this technology minimizing deposits and carbon buildup in equipment operating at high and low RPMs.

Bio-Fleet™ TC+ is recommended in both carbureted and Direct Fuel Injected (DFI) systems.  This ashless, Low-Smoke Formula contains Stabilized* Technology to improve fuel stability.

For premixed fuel-oil systems, see owner’s manual for recommended fuel: oil ratio.

Typical Characteristics

Physical Properties					Typical Value		Method

Viscosity, cSt 100°C				7.6			ASTM D-445

Viscosity, cSt 40°C					42.3			ASTM D-445

Viscosity Index					149			ASTM D-2270

Flash point, °C					98			ASTM D-93

TBN (mg KOH/g)					5.9			ASTM D-2896

Pour Point, °C					-33			ASTM D-97

Cloud point, °C					-11			ASTM D-2500

Brookfield @ -25°C, cP				<7500			ASTM D-2988

Biodegradability					>80%			CEC-L-33-A-94

Sulfated Ash					<0.001			ASTM D-874

Nitrogen	% wt.					  0.22			ASTM D-3228M

Bench & Engine Tests

Compatibility 					Pass			NMMA_CTCW

Filterability					Pass			NMMA_FPT

Fuel Miscibility					Pass			ASTM D-4682/#992

Rust						Pass			NMMA

Lubricity						Pass			AF-27

Piston Varnish					Pass

Piston Deposit					Pass

Ring Stick					Pass

Bearing Condition					Pass

Port Blocking					Pass

Scuffing						Pass

1 Readily Biodegradable >80% within 21 days in CEC L-33-T-82 test.

*STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.   Copyright 1999 Renewable Lubricants, Inc.

Availability    F.O.B. : Hartville, Ohio, USA     Quart    1 Gallon   5 Gallon Pail    Drum      Totes     Bulk

Product Item # 				85881     85883           85884           85886      85887    85889