### Bio-SynXtra™ TC+ 2-Cycle Engine Oil

# "Biobased Lubricants that Perform Like Synthetics"

Bio-SynXtra™ TC+ 2-Cycle Engine Oil is a patented, readily biodegradable1, biobased synthetic formula with improved additive technology that meets and exceeds API TC+ for high performance air-cooled 2 Cycle Engines.  This improved additive technology provides additional antiwear/anti-scuffing protection and is recommended for used in lawn and garden equipment, chain saws, snow blowers, motor scooters, mopeds, air-cooled snowmobiles, and air-cooled marine engines.  In addition, it meets and exceeds the National Marine Manufacturers Association (NMMA) requirements for obsolete Water-Cooled TC-W (BIA), TC-WII for older outboard 2-Cycle Engine.

Bio-SynXtra™ TC+ contains enhanced lubricity boosters and additional cleanliness chemistry that improves lubrication performance for high output Motorcycle API TC and Husqvarna Chain Saw 242/266 requirements.  It is specifically formulated to reduce visible smoke and burn clean, minimizing deposits and carbon buildup, and preventing ring sticking and spark plug fouling.  In addition, this technology minimizing deposits and carbon buildup in equipment operating at high and low RPMs.

Bio-SynXtra™ TC+ is recommended in both carbureted and Direct Fuel Injected (DFI) systems.  This ashless, Low-Smoke Formula contains Stabilized* Technology to improve fuel stability.

For premixed fuel-oil systems, see owner’s manual for recommended fuel: oil ratio.

Typical Characteristics

Property							Typical Value		Method

Viscosity, cSt 1000C				8.8			ASTM D-445

Viscosity, cSt 400C					48.1			ASTM D-445

Viscosity Index					164			ASTM D-2270

Flash point, 0C					180			ASTM D-93

TBN (mg KOH/g)					6.0			ASTM D-2896

Pour Point, 0C					-36			ASTM D-97

Cloud point, °C					-18			ASTM D-2500

Brookfield @ -25°C, cP				<7500			ASTM D-2988

Biodegradability					>80%			CEC-L-33-A-94

Sulfated Ash					<0.001			ASTM D-874

Nitrogen	% wt.					  0.22			ASTM D-3228M

Bench & Engine Tests

Compatibility 					Pass			NMMA_CTCW

Filterability					Pass			NMMA_FPT

Fuel Miscibility					Pass			ASTM D-4682/#992

Rust						Pass			NMMA

Lubricity						Pass			AF-27

Yamaha CE50S Tightening/Lubricity Test		3.90 / 4.37 / Pass		Equal to or better than reference ** OS250541

Torque Drop, lb-in. Candidate/Reference/Eval.				within 90% confidence level

1 Readily Biodegradable >80% within 21 days in CEC L-33-T-82 test.

*STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.   Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA     Quart    1 Gallon   5 Gallon Pail    Drum      Totes     Bulk

Product Item # 			       85211     85213           85214           85216      85217    85219