### Bio-Ultimax™ 2000 Hydraulic Fluids

### (AW ISO 32, 46, 68, 100)

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Ultimax™ 2000 Hydraulic Fluids are ultimately biodegradable1 biosynthetic formulas that directly replace mineral oil based hydraulic fluids.  These patented biobased hydraulic fluids are formulated to perform in high and low pressure hydraulic systems that require Anti-Wear (AW), anti-rust, anti-oxidation, anti-foam, and demulsibility properties.  They are highly inhibited against moisture and rusting in both fresh and sea water and pass A and B Sequences of the ASTM D-665 Turbine Oil Rust Test.  Incorporating the super high viscosity index (VI) of the Stabilized* High Oleic Base Stocks (HOBS) into the formulas, increases the viscosity index past synthetic levels (Energy Conserving Formulas).  The super high viscosity index of the HOBS naturally improves the thermal shear stability of the formula and increases load capacity.  The HOBS’s extremely low volatility increases the flash and fire safety features in the formula.  They are formulated to provide seal conditioning for longer seal life and to reduce oil leakage from the system.  They are compatible with the same seals, filters, materials and components that are designed to operate on petroleum oil based formulations.  An environmentally friendly, zinc-free additive system has also been developed that meets or exceeds high pressure pump requirements.

Bio-Ultimax™ Hydraulic Fluids have a long-term history of proven performance with over 15 years of successfully being used in a wide variety of stationary and mobile hydraulic equipment.  These patented super high VI fluids have performed successfully in hydraulic systems up to 10,000 psi and in systems with ultra-fine filtration.  They are designed for use in hydraulic vane, piston, and gear-type pumps that require DIN 51524 Part 2 and 3 (HLP/HVLP), Parker-Denison HF-O/T6H20C, HF-1, HF-2, Eaton-Vickers M-2950-S (35VQ-25) and I-286-S (V-104C), Rexroth, Sauer-Sundstrand, Bosch, Commercial Intertech,  GM (LS-2), US Steel 126, 136, and 127.  They also meet the requirements for ashless API GL-1, GL-2, GL-3, DIN 51517 Part 3, and AGMA Non-EP gear oils for bearings, reduction units, and gear sets where they meet the viscosity ranges.  They have shown to have exceptional anti-wear performance in ASTM D-4172 Four Ball Wear Tests.  Very little wear was encountered in the field studies and in accelerated pump tests using biobased formulations in Denison T-5D, Vickers 20VQ, 35VQ-25 (M-2950-S), and V-104C (ASTM D-2882), Vickers I-286-S pump stand tests at pressures and temperatures ranging from 2000 to 3000 psi and from 1500 to 2100 F.  Their anti-wear performance exceeds the requirements for GM (LS-2), US Steel 126, 136 and 127, and load stage 10 in the FZG (DIN 51354).  Bio-Ultimax™ Hydraulic Fluids meets and exceeds Federal Specifications A-A-59354 Superseding MIL-H-46001D Specification for machine tool hydraulic systems.

Bio-Ultimax™ 2000 Hydraulic Fluids meet the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used in hydraulic systems where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  They exceed the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Because they meet the environmental requirements they can also be used where ISO 15380 (HEES/HETG) Hydraulic Fluids are specified. Bio-Ultimax™ Hydraulic Fluids are ENVIRONMENTALLY ACCEPTED LUBRICANTS (EALs) that are formulated from renewable biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate / Readily Biodegradation Pw1 >60% within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants™ is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Bio-Ultimax™ 2000 Hydraulic Fluids ISO 32, 46, 68, 100

Bio-Ultimax™ 2000 Hydraulic Fluids are designed to provide high performance in the high temperature/high pressure machine tool environment.  In machine tool equipment, the hydraulic pump may work continuously in automatic machines.  Machines may run 24 hours and 7 days a week non-stop.  Close tolerances (0.00015 in. = 3 micron) and fine system filters (3 to 5 absolute filtration) for hydraulic/electric servo drive systems can work to elevate hydraulic system temperatures rapidly.  It is also not unusual for hydraulic system components to be located close to very high temperature areas, i.e., on the side of a plastic mold injection gun.  The very high oxidative stability of Bio-Ultimax™ 2000 Hydraulic Fluids meets these demands.  Bio-Ultimax™ 2000 exceeds the requirements for DIN 51524 Part 2 and 3.

| TYPICAL SPECIFICATIONS | METHOD | ISO 32 | ISO 46 | ISO 68 | ISO 100 | Spec. Requirements |
| --- | --- | --- | --- | --- | --- | --- |
| Specific Gravity @ 15.6°C Viscosity @ 40°C Viscosity @ 100°C Viscosity @ -15°C, Brookfield Viscosity @ -25°C, Brookfield Viscosity Index | ASTM D-287 ASTM D-445 ASTM D-445 ASTM D-2983 ASTM D-2983 ASTM D-2270 | 0.89 29.6 6.5 530 cP 1,180 cP 183 | 0.89 44.4 8.9 690 cP 1,600 cP 186 | 0.90 64.5 12.1 1,270 cP 3,600 cP 188 | 0.90 92.9 16.3 3,200 cP 4,400 cP 189 | Report Note 1 Note 1 Note 1 Note 1 90 (min) |
| Pour Point Flash Point (COC) Fire Point (COC) Hydrolytic Stability, Copper Wt. Loss (mg) Copper Appearance Water Layer Foam Sequence I, II, III (10 min) Rust Prevention Distilled Water Syn. Sea Water | ASTM D-97 ASTM D-92 ASTM D-92 ASTM D-2619 ASTM D-892 ASTM D-665 | -46°C 240°C 265°C 0.0417 1A 3.0 0 Foam Pass Pass | -45°C 244°C 272°C 0.0208 1B 3.0 0 Foam Pass Pass | -42°C 253°C 275°C 0.0208 1B 3.0 0 Foam Pass Pass | -40°C 254°C 279°C 0.0208 1A 3.6 0 Foam Pass Pass | Note 1 198°C (min) 218°C (min) 0.2 Report 4 150/0, 80/0, 150/0 Pass Pass |
| Copper Corrosion Strip 3hr @ 100°C | ASTM D-130 | 1A | 1A | 1A | 1 A | DIN 51524 2(max) |
| RPVOT, (minutes) Dielectric Strength (KV) (Avg) Oxidation Stability (Pressure Differential Scanning Calorimeter) min Neutralization Number mg KOH/g Swell of Synthetic NBR-L Rubber, % (Avg.) Volume Change (%) Shore A Hardness Change (%) Filterability A-No Water (s) (Avg) B-2% Water (s) (Avg) Demulsibility, ML Oil/Water/Emulsion 4-Ball Wear, 1h, 167°F, 1200 RPM, 40 kg FZG Test A/8,3/90 | ASTM D-2272 ASTM D-877 ASTM D-5483 Modified ASTM D-974 DIN 53538, Part 1 Denison TP 02100 HF-0 Requirement ASTM D-1401 ASTM D-4172 DIN 51354 Part 2 | >600 42 90 (165°C) <0.4 9.0 -5 113 187 40/ 40/ 0 (<10 minutes) 0.3 – 0.4 12 | >600 40 90 (165°C) <0.4 9.0 -5 335 449 40/ 40/ 0 (<10 minutes) 0.3 – 0.4 12 | >600 40 90 (165°C) <0.4 9.0 -5 335 449 40/ 40/ 0 (<10 minutes) 0.3 – 0.4 12 | >550 40 90 (165°C) <0.4 9.0 -5 355 470 40/40/0 (<10 minutes) 0.3 – 0.4 12 | USS 120 (min) >35 Note 2 1.5 (max) 0 to 12 0 to -7 600 (max) 2xA (max) 40/37/3 (max) (30 minutes) USS 127 0.5 (max) US.Steel 10 (min) |
| Biodegradation Classification Environmentally Friendly USDA Biobased Tested Environmental Management System Ecotoxicity LC-50 / EC-50 Note 1 Viscosity Sufficient for Application Note 2 Not Required RLI Product Item # | ASTM D-5864 OECD 301B ISO 15380 New Carbon ISO 14001 EPA 560/6-82-002, 003 | Ultimate PW1 Readily yes meets/exceeds yes meets/exceeds 81100 | Ultimate PW1 Readily yes meets/exceeds yes meets/exceeds 81110 | Ultimate PW1 Readily yes meets/exceeds yes meets/exceeds 81120 | Ultimate PW1 Readily yes meets/exceeds yes meets/exceeds 81130 | Ultimate PW1 Readily yes meets/exceeds (Over 50%) yes meets/exceeds |

If oil samples are monitored and if the machine is running under clean conditions, fluid life can be increased with improved oxidation stability and proper lubricant filtration.  Even though the US Steel requirement is a minimum of 125 minutes in the RPVOT, the hydraulic system’s fluid life can be increased considerably when RPVOT exceeds 400 minutes and a proper preventative maintenance sampling program is used.  General Electric, GEK 32568A, requires an RPVOT minimum of 450 minutes in turbine oil requirements.  With Bio-Ultimax™ 2000 Hydraulic Fluids, an RPVOT of over 600 minutes has been met that increases fluid and equipment life.

Availability	F.O.B.: Hartville, Ohio, USA    1 Gallon   5 Gallon Pail  Drum  Totes  Bulk