### Bio-Bottle JackTM Hydraulic Fluid

### (ISO 32)

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Bottle JackTM Hydraulic Fluid is a biobased, biodegradable and environmentally non-toxic hydraulic oil for use in general purpose hydraulic systems.  This patented ISO 32 viscosity grade hydraulic oil is specially designed to be a direct replacement for petroleum oil based hydraulic fluids in mobile and stationary hydraulic vane, piston and gear type pumps.  This patented technology provides superior oxidation stability and longer fluid life compared to other vegetable based hydraulic oils.  It meets or exceeds the requirements for Type I, II and III hydraulic tools.

Bio-Bottle JackTM Hydraulic Fluid is ultimately biodegradable1 vegetable based formula that meets and exceeds Vickers M-2950-S, Vickers 1-286-5, U.S. Steel 126, and U.S. Steel 127.  This patented bio-renewable hydraulic fluid is formulated to perform in fleet, marine, and industrial hydraulic systems that require Anti-Wear (AW), anti-rust, anti-oxidation, anti-foam, and demulsibility properties.  An environmentally friendly, zinc-free additive system has also been developed that meets or exceeds high pressure pump requirements.  The anti-wear performance meets the requirements for Vickers 35VQ-25 and V-104C (ASTM D-2882) vane pump stand tests, and exceeds DIN 51524 Part 2 load stage 10 that is recommended for piston and gear pumps.

Bio-Bottle JackTM Hydraulic Fluid is the perfect economical choice for hydraulic equipment operating outside, where unpredictable higher moisture and dusty environments are more prominent and the equipment require more frequent oil change intervals.  It is highly inhibited against moisture and rusting in both fresh and sea water, passed both A and B Sequences of the ASTM D-665 Turbine Oil Rust Test and provides excellent water separation as shown in ASTM D-1401 Demulsibility Test.

Incorporating the super high viscosity index (VI) of the Stabilized* High Oleic Base Stocks (HOBS) into the formula, increases the VI past synthetic levels (Energy Conserving Formulas).  In addition, this super high VI naturally improves the thermal and mechanical shear stability of the formula and provides additional fluid protection under higher loads and pressures.  The HOBS’s extremely low volatility increases the flash and fire safety features in the formula.  This biobased fluid is designed to provide seal conditioning for longer seal life and to reduce oil leakage from the system.

Bio-Bottle JackTM Hydraulic Fluid meets the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used in hydraulic systems where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  This product exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Bottle JackTM Hydraulic Fluid is an ENVIRONMENTALLY RESPONSIBLE lubricant that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants™,* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

Trademark of Renewable Lubricants™, Inc.   Copyright 1999 Renewable Lubricants™ Inc.

Availability	F.O.B. :Hartville, Ohio, USA	1 Quart   1 Gallon   5 Gal Pail    Drum   Totes    Bulk

Item #:						81631	     81633         81634      81636    81637   81639

PRODUCT BENEFITS

 Specially designed to be compatible with petroleum hydraulic fluid and their systems and existing equipment may be “topped off”.    (Safe for use with Buna N, Viton, Neoprene Elastomers)

 Lubricates		 Improved oxidation stability	 Prevents Rust   	 Renewable

 Non-foaming		 Maintains viscosity		 Biobased, Biodegradable, Eco Non-toxic

 Low temperature performance 	 Excellent anti-wear

TYPICAL APPLICATIONS

 Hydraulic vane, piston and gear pumps		 Fork lift gates	 Floor lifts

 Floor jacks		 Hydraulic hand jacks		 Hydraulic lift gates	 Pallet jacks

 Tilt cab systems	 ISO 32 specified hydraulic applications		 Safety gates

 Jack stand								             Stadium gates

### Bio-Bottle JackTM Hydraulic Fluid ISO 32

| TYPICAL SPECIFICATIONS | METHOD | ISO 32 | Spec. Requirements |
| --- | --- | --- | --- |
| Specific Gravity @ 15.6°C Viscosity @ 40°C Viscosity @ 100°C Viscosity @ -25°C, Brookfield Viscosity Index | ASTM D-287 ASTM D-445 ASTM D-445 ASTM D-2983 ASTM D-2270 | 0.88 30.5 6.7 1,400 cP 186 | Report Note 1 Note 1 Note 1 90 (min) |
| Pour Point Flash Point (COC) Fire Point (COC) Foam Sequence I, II, III (10 min) Rust Prevention Distilled Water Syn. Sea Water | ASTM D-97 ASTM D-92 ASTM D-92 ASTM D-892 ASTM D-665 | -35°C 232°C 255°C 0 Foam Pass Pass | Note 1 198°C (min) 218°C (min) 0 Foam Pass Pass |
| Copper Corrosion Strip 3hr @ 100°C | ASTM D-130 | 1A | DIN 51524 2(max) |
| Rotary Bomb Oxidation, (minutes) Neutralization Number mg KOH/g Swell of Synthetic NBR-L Rubber, % (Avg.) Volume Change (%) Shore A Hardness Change (%) Demulsibility, ML Oil/Water/Emulsion 4-Ball Wear, 1h, 167°F, 1200 RPM, 40 kg FZG Test | ASTM D-2272 ASTM D-974 DIN 53538, Part 1 ASTM D-1401 ASTM D-4172 DIN 51354 | 272 0.5 6.0 -4 40/ 40/0 <10 minutes 0.40 11 | USS 120 (min) 1.5 (max) 0 to 12 0 to -7 40/37/3 (max) (30 minutes) USS 127 0.5 (max) US.Steel 10 (min) |
| Biodegradation Classification Environmentally Friendly USDA Biobased Tested Note 1 Viscosity Sufficient for Application Note 2 Not Required | ASTM D-5864 OECD 301B ISO 15380 New Carbon | Ultimate PW1 Readily yes yes | Ultimate PW1 Readily meets/exceeds over 50% |