### Bio-SynXtra™ Marine Hydraulic Fluids

### ISO 15380 HEES, AW ISO 32, 46, 68, 100

# "Biobased Lubricants that Perform Like Synthetics"

Bio-SynXtra™ Marine Hydraulic Fluids were designed specifically to provide exceptional international Environmentally Acceptable Lubricants (EAL) performance for world-wide marine applications in international waters.  They are ultimately biodegradable1, fully saturated biosynthetic HEES formulas that meet both European EU Ecolabel** and US Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for EALs.  These high performance hydraulic fluids are formulated to readily biodegrade and offer low toxicity in aquatic conditions.  An environmentally friendly, zinc-free (ash-less) additive system has also been developed that meets or exceeds pump requirements.  They can be used in a wide variety of stationary and mobile hydraulic equipment, and these fully saturated ester formulas provide excellent pump lubrication and filterability under normal and abnormal wet conditions.

Bio-SynXtra™ Marine Hydraulic Fluids directly replace petroleum based hydraulic fluids and provide exceptional performance in high and low pressure hydraulic systems that require Anti-Wear (AW), anti-rust, anti-oxidation, anti-foam, and rapid demulsibility properties. They are highly inhibited against moisture and rusting in both fresh and sea water and pass A and B Sequences of the ASTM D-665 Turbine Oil Rust Test.  The high viscosity index of these biosynthetic formulas improves mechanical and thermal shear stability and provides additional fluid value at higher temperatures and pressures.  The formulas provide seal conditioning for longer seal life and reduce oil leakage from the system.

Bio-SynXtra™ Marine Hydraulic Fluids provide exceptional protection in hydraulic equipment operating over a wider range of temperatures and environmental conditions.  They are recommended for use in hydraulic vane, piston, and gear-type pumps that require DIN 51524 Part 2 and 3, Parker-Denison HF-O, HF-1, HF-2, Eaton-Vickers M-2950-S (35VQ-25) and I-286-S (V-104C), Rexroth, Sauer-Sundstrand, GM (LS-2), US Steel 126, 136, and 127.  They also meet the requirements for ashless API GL-1, GL-2, GL-3, DIN 51517 Part 3, and AGMA Non-EP gear oils for bearings, reduction units, and gear sets where they meet the viscosity ranges.

Bio-SynXtra™ Marine Hydraulic Fluids are recommended for use with Viton fluorocarbon (FKM 2), fluorosilicone, Teflon (PTFE), Polyurethane (AU), polysulfide, Buna-N (NBR1) and Hydrogenated Nitrile Buna Rubber (HNBR).  They are compatible with the same seals, filters, materials and components that are designed to operate on petroleum oil based formulations.  They are not recommended for use where neoprene, natural rubber, and styrene-butadiene rubber (SBR, Buna S) seals are used.

Bio-SynXtra™ Marine Hydraulic Fluids meet the EPA 2013 VGP definition for EALs, and should be used in hydraulic systems where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  They exceed the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-SynXtra™ Marine Hydraulic Fluids are ENVIRONMENTALLY ACCEPTED LUBRICANTS (EALs) that are formulated from renewable biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate/Readily Biodegradation Pw1biodegradable >60% within 28 days in OECD 301B and ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

*STABILIZED by Renewable Lubricants™ is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  This Stabilized technology provides a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

™ Trademark of Renewable Lubricants™, Inc. on their Proprietary Formulas.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B.: Hartville, Ohio, USA    5 Gallon Pail    Drum   Totes   Bulk

Bio-SynXtra™ Marine Hydraulic Fluids are not a stocked product.

(Contact RLI for product order information).

Bio-SynXtra™ Marine Hydraulic Fluids ISO 32, 46, 68, 100

The test data below show that the Bio-SynXtra™ Marine Hydraulic Fluids are designed to provide exceptional high performance in a wide variety of stationary and transportation equipment that operate in broad ranges of environmental conditions.  In equipment operating outside, wear from poor cold temperature pumpability, surge loads, moisture, and dusty environments are more prominent.  Bio-SynXtra™ Marine Hydraulic Fluids are formulated to improve performance in equipment that requires excellent anti-wear, anti-corrosion, anti-foam, oxidation stability, rapid water separation, cold temperature pumpability and filterability.

| TYPICAL SPECIFICATIONS | METHOD | ISO 32 | ISO 46 | ISO 68 | ISO 100 | Spec. Requirements |
| --- | --- | --- | --- | --- | --- | --- |
| Viscosity @ 40°C | ASTM D-445 | 32.7 | 44.7 | 66.3 | 96.6 | Note 1 |
| Viscosity @ 100°C | ASTM D-445 | 6.2 | 8.3 | 11.3 | 15.3 | Note 1 |
| Viscosity @ 0°C | ASTM D-445 | 270 cP | 366 cP | 564 cP | 874 cP | Note 1 |
| Viscosity @ -20°C, Brookfield | ASTM D-2983 | 1470 cP | 1950 cP | 3100 cP | 4990 cP | Note 1 |
| Viscosity Index | ASTM D-2270 | 151 | 163 | 165 | 168 | 140 (min) (DIN ISO 2909) |
| Dielectric Strength, KV (Avg) | ASTM D-877 | >40 | >40 | >40 | >40 | 35 (min) |
| Pour Point | ASTM D-97 | -48°C | -46°C | -43°C | -41°C | -39°C to -18°C (min) (DIN ISO 3016) |
| Flash Point | ASTM D-92 | 231°C | 260°C | 278°C | 275°C | 175-195°C (min) (DIN EN ISO 2592) |
| Water Content % | DIN EN ISO 12397 | <.05 | <.05 | <.05 | <.05 | .05% (max) |
| Foam Sequence I, II, III | ASTM D-892 | < 30/0 Foam | < 30/0 Foam | < 30/0 Foam | < 30/0 Foam | 150/0, 80/0, 150/0 (DIN EN ISO 6247) |
| Air Release Value (minutes) | ASTM D-3427 | 2 | 2 | 3 | 4 | 10 (max) (DIN 51381 ISO 9120) |
| Rust Prevention | ASTM D-665 |  |  |  |  |  |
| Distilled Water |  | Pass | Pass | Pass | Pass | (DIN ISO 7120) Pass |
| Syn. Sea Water |  | Pass | Pass | Pass | Pass | Pass |
| Copper Corrosion, 3hr @ 100°C | ASTM D-130 | 1B | 1B | 1B | 1B | DIN 51524 (2 max) (DIN EN ISO 2160) |
| Oxidation Dry TOST, hrs. | ASTM D-943 | >7000 | >7000 | >6000 | >5000 | Note 2 |
| Oxidation RPVOT, (minutes) | ASTM D-2272 | >1000 | >1000 | >900 | >700 | USS 120 (min) |
| Baader Test (72 hrs @ 110°C) KV 40°C % change | DIN 51554-3 | < 2 | < 2 | < 3 | < 3 | 20% (max) |
| Demulsibility, ML Oil/Water/Emulsion | ASTM D-1401 | (<10 minutes) 40/40/0 | (<10 minutes) 40/40/0 | (<10 minutes) 40/40/0 | (<10 minutes) 40/40/0 | 40/37/3 (30 minutes) (DIN ISO 6614) |
| 4-Ball Wear, 1h, 167°F, 1200 RPM, 40 kg (mm) | ASTM D-4172 | 0.4-0.5 | 0.4-0.5 | 0.4-0.5 | 0.4-0.5 | USS 127 0.5 (max) |
| FZG Test A/8.3/90 Fail load stage | DIN ISO14635-1 | 12 | 12 | 12 | 12 | 10 (min) |
| V104C Vane Pump Low total wear avg. 5 to 15 mg | ASTM D-2882 ISO 20763 | Pass | Pass | Pass | Pass | Ring loss 120 mg (max) Vane loss 30 mg (max) |
| Biodegradation Classification | ASTM D-5864 OECD 301B | Ultimate Pw1 Readily | Ultimate Pw1 Readily | Ultimate Pw1 Readily | Ultimate Pw1 Readily | Ultimate PW1 Readily |
| Environmentally Friendly | ISO 15380 | yes | yes | yes | yes | meets/exceeds |
| BioPreferred | USDA Biobased | yes | yes | yes | yes | meets/exceeds |
| Environmental Management System | ISO 14001 | yes | yes | yes | yes | meets/exceeds |
| Ecotoxicity LC-50/EC-50 See SDS | EPA 560/6-82-002, 003 | yes | yes | yes | yes | meets/exceeds |
| Vessel General Permit | US EPA VGP | yes | yes | yes | yes | meets/exceeds |
| Ecolabel Performance ** | Europe | yes | yes | yes | yes | meets/exceeds |
| Product Item # |  | 80850 | 80860 | 80870 | 80880 | -- |

Bio-SynXtra™ Marine Hydraulic Fluids are not a stocked product.

Note 1      Viscosity Sufficient for Application

Note 2      Not Required

Note  ** EU Ecolabel Certification can be purchased for label branding, based on order volumes.

(Contact RLI for product order information).