### Bio-SynXtraTM Trans-Hydraulic

#### (All-Weather Super Universal Tractor Fluid)

# "Biobased Lubricants that

# Perform Like Synthetics"

Bio-SynXtra™ Trans-Hydraulic is a universal tractor fluid (UTF) that incorporates Stabilized* additive technology with biodegradable1 biobased / bio-synthetic based stocks for improved performance over conventional tractor oils.  This multi-grade formulation contains special frictional modifiers for the Wet Brake’s equipment design, and compounded with detergent, dispersant, anti-wear, anti-rust, and anti-foam inhibitors.  Bio-SynXtra™ Trans-Hydraulic Fluid is a multi-purpose all-weather super tractor hydraulic fluid that can commonly be used in farm and construction equipment, off-highway vehicles, industrial tractors used in agricultural, industrial, and construction equipment, with proven field performance.

Although it may differ from manufacturers’ recommended fluids, Bio-SynXtra™ Trans-Hydraulic Fluid has been highly tested, Tractor Life.com Authenticated, and can be used to meet or exceed all of the following performance specifications.; Allison C-3, Cat TO-2 and API GL-4, FZG/Low-Speed/High Torque, J20-C/M1139 High Torque Axle, Wet Brake Chatter/Squawk, PTO Clutch, the North America Performance Requirements for Universal Tractor Transmission Oils (UTTOs), and Multipurpose Tractor Oils (MTO)

Biodegradable Tractor Transmission Oil Providing Excellent Performance, and suitable and commonly used in the following Tractor specifications:

Ford, New Holland	M2C134-D, FNHA-2-201, M2C86-C, M2C86-C/B, **M2C41-B/A, M2C48-C/B, M2C92-A, M2C53-B/A, M2C134-C/B/A,

CNH MAT 3525

Massey-Ferguson	M1135, M1141, M1139, M1143, M1145, **M1110, M1127B/A, M1129A

Kubota, 	UDT, Super UDT

John Deere	J20C, J14A/B/C, **J20D

Steiger, 		SEMS 1700A

Versatile, 	28M, 24M

Case International

**JIC-145/MS-1210

JIC-185/MS-1204, MS-1205, MS-1206

MS-1207, MS-1209, MS1127, M1129-A

Agco, White Farm

Q-1826 Q-1705, Q-1766, Q-1802, Type 55

Agco, Deutz-Allis 821XL

Landini

Fiat-Hesston, AF-87, Multi-F

TRANSMISSION OEM’S

**J20C spec for Allison C4

Caterpillar TO-2, MTO

Hydraulic: Vickers, Denison, Commercial Intertech, Rexroth, Sauer-Sundstrand

**Lower viscosity specifications can be replaced where recommended.

Bio-SynXtra™ Trans-Hydraulic meets the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used in hydraulic systems where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  This product exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-SynXtra™ Trans-Hydraulic is an ENVIRONMENTALLY ACCEPTED LUBRICANT (EAL) that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate/Readily Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants™* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high-performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants™,  Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B.: Hartville, Ohio, USA      1 Gallon   5 Gallon Pail    Drum     Totes      Bulk

RLI Product Item #			               81223	     81224            81226     81227     81229

## Test					Typical Results		Specification Limits

SAE Grade:					5W30

Viscosity @ 100°C ASTM D-445	SAE 30=	9.72			9.10 min.

Viscosity @ 40°C ASTM D-445			46.38			Report

Viscosity @ 25°C ASTM D-445			82.9			Report

Viscosity Index ASTM D-2270			202			140

Shear Stability Orbahn ASTM D-6278

Vis. @ 100°C (after shear)			9.6			9.10 min.

Brookfield Viscosity ASTM D-2983

@-20°C 1,500 cP per J20D		 1,200 cP		5,500 max.

@-35°C					10,500 cP		70,000 max.

@-40°C 20,000 cP per J20D 		18,500 cP		20,000 max.

Flash Point, °C  (ASTM D-92)			252			200 min.

Stable Pour Point, °C  (ASTM D-97)		-45			-36 max.

Rust Prevention A&B,  (ASTM D-665)		Pass Clean 		No Visible Rust

Acid Number, mg KOH / g  (ASTM D-974)		0.56			Report

Dielectric Strength (ASTM D-877)			48 KV			35 KV (Minimum)

Four Ball Wear (ASTM D-4172)

1 h, 65°C, 1500 rpm, 40 kg,  			0.36			0.40 max.

Oxidation Stability JDQ 16

Evaporation Loss				0.85%			5.0% max.

Viscosity Increase @ 100°C		3.0%			10.0% max.

Viscosity Increase @ 40°C		3.8%			--------

Sludge Formation				None			None

Additive Separation 			None			None

Rust Protection JDQ 22				>100			100 hrs. min.

Copper Corrosion JDQ 32				1A			1B max.

Foaming Characteristics JDQ 33

Sequence I				0/0			25/0 ml. max.

Foam Breaktime				0			30 sec. max.

Sequence II				40/0			50/0 ml. max.

Foam Breaktime				0			30 sec. max.

Sequence III				0/0			25/0 max.

Foam Breaktime				0			30 sec. max.

Water Sensitivity JDQ 19

Solids 					0.0			0.1 %v max.

Additive Loss				0.0			15.0% wt. max.

Extreme Pressure Properties JDQ 34

Timken Abrasion Mass Loss		0.5 mg.			1.5 mg. max

Timken OK Load				73 N			45 N min.

##### Rubber Compatibility JDQ 9

Volume Change				+2			0 to +5%

Hardness Change				 -1			0 to  -5 pts.

Precipitation				None			Trace

Rubber Compatibility

Reference 69X311111

Volume Change				+3			0 to +5

Hardness Change				-1.5			0 to –5

Precipitation				None			None

Oil Compatibility JDQ 23

Additive Separation			None			None

Formation				None			None

Low Temperature Fluidity JDQ 73/74

Cold Soak @ -35°C				20 secs.			30.0 sec. max.*

Slow Cool

@ -30°C					30 mm in 3 sec.		30.0 sec. max.*

@ -35°C flow in 30 sec.			30 mm in 11 sec.		10.0 mm min.**

*Must flow 30 mm in a maximum of 30 seconds to pass.

## Test					Typical Results		Specification Limits

##### JDQ 94 PST Clutch Friction

Total Cycles					2,000			2,000

Initial Friction Coefficient				0.077			0.15 max.

Final Friction Coefficient				0.105			0.08 min.

Stall Time (sec.)					1.77			5.0 max.

Disk #1 Wear (mm)				0.178			0.38 max.

Disk #2 Wear (mm)				0.174			0.38 max.

Disk #3 Wear (mm)				0.254			0.38 max.

Disk #4 Wear (mm)				0.178			0.38 max.

JDQ 102 Shear Stability

Viscosity @ 100°C			9.8

Viscosity @ 100°C (sheared)		9.4

% Viscosity Loss				6.0%

JDQ 95 Spiral Bevel/Final Drive Gear Wear

Gear Surface Condition

Pinion				None			No Scoring

Ring				None			No Scoring

Spiral Bevel Rating				9			Scale of 1-10,

10 = the best

Sun Pinion Wear

Left Side Average			<0.025			<0.025

Right Side Average             		<0.025			<0.025

###### JDQ 84 Sundstrand Hydraulic Pump

Flow Degradation			Better than reference		Equal to or better

than reference which

is –2.0%.

JDQ 96 Brake Torque Variation and Friction

Computer Results		Torque			SwRI

Cycles			Relative Capacity		Variation		Variation

1,000			293,131			44,470			559,780

10,000			308,090			36,730			424,130

20,000			310,651			36,220			421,620

30,000			312,768			42,380			506,220

Total			1,224,640		159,800			1,911,750

###### Allison C-4 Oxidation Test (J20C Spec.)

Tan Increase				5.0				7.0 max.

Carbonyl Absorbance			0.9				0.9 max.

Front Pump Seal				Moderate-			Moderate to

Hardening			Heavy Hardening

Light Sludge			Light to Medium Sludge

Allison C-4 Wear Test

Total weight loss				1.4 mg				15.0 max.

Allison C-4 Paper Clutch Friction test

<=5,000   >5,000			<=5,000   >5,000

Cycles				Cycles

Slip Time, max.				0.70	0.55			0.72	0.61

Mid-Point Friction Coeff. min.		0.076	0.095			0.068	0.088

Allison C-4 Graphite Clutch Friction Test

1,500				5,500										Cycles

Slip Time, max.				0.70		0.74		0.71 max.

Mid-Point Friction Coeff. min.		0.101		0.097		0.104 min.

Biodegradability	CEC-L33A93		>80%				80% or greater

OECD 301B Mod. Sturm	>60%				60% or greater

ASTM D-5864		>60%				60% or greater

Ecotoxicity

Fathead minnow, 96h LC50, 	>2000 ppm			EPA requirement >1000

Daphnia magna, 48h EC50,	>2000 ppm			EPA requirement >1000

Alga Growth Inhibition EC50	>2000 ppm			EPA requirement >1000

Meets EPA requirements 560/6-82-002, 560/6-82-003

Energy Conserving Formulation – USDA Biobased and BioPreferred

Additional Benefits:

* Biodegradability

* Eco-nontoxicity

*Improved cold weather performance

*Excellent oxidation stability

*Enhanced efficiency in synchronised and glide shift transmissions

*Interchangeable with standard UTTO’s

*Improved performance over conventional UTTO’s

* High Flash Point / More Fire Resistant

* Eco-nontoxicity

* USDA Biobased

* BioPreferred