### Bio-Fleet™ Trans-Hydraulic

#### (Universal Tractor Fluid)

# "Biobased Lubricants that

# Perform Like Synthetics"

Bio-Fleet™ Trans-Hydraulic is a universal tractor fluid (UTF) that incorporates Stabilized* additive technology with biodegradable1 biobased oils.  It provides improved performance, provides efficiency in synchronised and glide shift transmissions, and is interchangeable with standard UTF.  This formulation contains special frictional modifiers for the Wet Brake’s equipment design, and is compounded with detergent, dispersant, anti-wear, anti-rust, and anti-foam inhibitors.  Bio-Fleet™ Trans-Hydraulic fluid is a multi-grade lubricant that can be used in agricultural, industrial, and construction equipment and has proven field performance.

Although it may differ from manufacturers’ recommended fluids, Bio-Fleet™ Trans-Hydraulic Fluid has been highly tested, Tractor Life.com Authenticated, and can be used to meet or exceed all of the following performance specifications: Allison C-3, Cat TO-2 and API GL-4, FZG/Low-Speed/High Torque, J20-C/M1139 High Torque Axle, Wet Brake Chatter/Squawk, PTO Clutch, the North America Performance Requirements for Universal Tractor Transmission Oils (UTTOs), and Multipurpose Tractor Oils (MTO)

Biodegradable Tractor Transmission Oil Providing Excellent Performance, and suitable and commonly used in the following Tractor specifications: Bio Fleet UTF is usually recommended in moderate temperature applications (-35°C to 80 °C with a maximum temperature of 80 °C (176°F).

Ford, New Holland

M2C134-D, FNHA-2-201

M2C86-C, M2C86-C/B

**M2C41-B/A, M2C48-C/B, M2C92-A

M2C53-B/A, M2C134-C,B,A

CNH MAT 3525

Massey-Ferguson

M1135, M1141, M1139, M1143, M1145,

**M1110, M1127B/A, M1129A

John Deere J20C, J14A/B/C, **J20D

Kubota, UDT

Steiger, SEMS 1700A

Versatile, 28M, 24M

Case International

**JIC-145/MS-1210

JIC-185/MS-1204, MS-1205, MS-1206

MS-1207, MS-1209, MS1127, M1129-A

Agco, White Farm

Q-1826 Q-1705, Q-1766, Q-1802, Type 55

Agco, Deutz-Allis 821XL

Landini

Fiat-Hesston, AF-87, Multi-F

TRANSMISSION OEM’S

**J20C spec for Allison C4

Caterpillar TO-2

Hydraulic: Vickers, Denison, Commercial Intertech, Rexroth, Sauer-Sundstrand

**Lower viscosity specifications can be replaced where recommended by OEM.

Bio-Fleet™ Trans-Hydraulic meets the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  This product exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Fleet™ Trans-Hydraulic is an ENVIRONMENTALLY ACCEPTED LUBRICANT (EAL) that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants™* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants™, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B.: Hartville, Ohio, USA	1 Gallon  5 Gallon Pail    Drum     Totes      Bulk

RLI Product Item #				  81203	        81204          81206     81207     81209

## Test					Typical Results		Specification Limits

Viscosity @ 100°C ASTM D-445		10.26				9.10 min.

Viscosity @ 40°C ASTM D-445		47.8				Report

Viscosity Index ASTM D-2270		210				140

Shear Stability Orbahn ASTM D-6278

Vis. @ 100°C (after shear)		9.6				9.10 min.

Brookfield Viscosity ASTM D-2983

@-20°C				1,650				5,500 max.

@-35°C				21,150				70,000 max.

Flash Point, °C  (ASTM D-92)		251				200 min.

Stable Pour Point, °C  (ASTM D-97)		-39				-36 max.

Rust Prevention A&B,  (ASTM D-665)		Pass Clean 			No Visible Rust

Acid Number, mg KOH / g  (ASTM D-974)	0.6				Report

Dielectric Strength (ASTM D-877) 46 KV 35 KV (Minimum)

Four Ball Wear (ASTM D-4172)

1 h, 65°C, 1500 rpm, 40 kg,  			0.36				0.40 max.

Oxidation Stability JDQ 16

Evaporation Loss			0.65%				5.0% max.

Viscosity Increase @ 100°C		5.02%				10.0% max.

Viscosity Increase @ 40°C		4.0				--------

Sludge Formation			None				None

Additive Separation 		None				None

Rust Protection JDQ 22			>100				100 hrs. min.

Copper Corrosion JDQ 32			1A				1B max.

Foaming Characteristics JDQ 33

Sequence I			0/0				25/0 ml. max.

Foam Breaktime			0				30 sec. max.

Sequence II			50/0				50/0 ml. max.

Foam Breaktime			0				30 sec. max.

Sequence III			0/0				25/0 max.

Foam Breaktime			0				30 sec. max.

Water Sensitivity JDQ 19

Solids 				0.0				0.1 %v max.

Additive Loss			0.0				15.0% wt. max.

Extreme Pressure Properties JDQ 34

Timken Abrasion Mass Loss		0.5 mg.				1.5 mg. max

Timken OK Load			73 N				45 N min.

##### Rubber Compatibility JDQ 9

Volume Change			+1				0 to +5%

Hardness Change			-0.5				0 to –5 pts.

Precipitation			None				Trace

Rubber Compatibility

Reference 69X311111

Volume Change			+2.5				0 to +5

Hardness Change			-1.5				0 to –5

Precipitation			None				None

Oil Compatibility JDQ 23

Additive Separation		None				None

Oxidation Stability

Evaporation Loss			1.6				5.0% max.

Viscosity Increase @ 100°C		6.0				10.0% max.

Viscosity Increase @ 40°C		9.8				---------

Sludge Formation			None				None

Additive Separation		None				None

Low Temperature Fluidity JDQ 73/74

Cold Soak @ -35°C			27 secs.				30.0 sec. max.*

Slow Cool

@ -30°C				30 mm in 3 sec.			30.0 sec. max.*

@ -35°C flow in 30 sec.		30 mm in 11 sec.			10.0 mm min.**

*Must flow 30 mm in a maximum of 30 seconds to pass.

## Test					Typical Results		Specification Limits

##### JDQ 94 PST Clutch Friction

Total Cycles				2,000				2,000

Initial Friction Coefficient			0.077				0.15 max.

Final Friction Coefficient			0.105				0.08 min.

Stall Time (sec.)				1.77				5.0 max.

Disk #1 Wear (mm)			0.178				0.38 max.

Disk #2 Wear (mm)			0.174				0.38 max.

Disk #3 Wear (mm)			0.254				0.38 max.

Disk #4 Wear (mm)			0.178				0.38 max.

JDQ 102 Shear Stability

Viscosity @ 100°C			10.51

Viscosity @ 100°C (sheared)		9.38

% Viscosity Loss			10.8%

JDQ 95 Spiral Bevel/Final Drive Gear Wear

Gear Surface Condition

Pinion				None				No Scoring

Ring				None				No Scoring

Spiral Bevel Rating				9				Scale of 1-10,

10 = the best

Sun Pinion Wear

Left Side Average			<0.025				<0.025

Right Side Average             		<0.025				<0.025

###### JDQ 84 Sundstrand Hydraulic Pump

Flow Degradation				3.9%				Equal to or better

than reference which

is –2.0%.

JDQ 96 Brake Torque Variation and Friction

Computer Results		Torque			SwRI

Cycles			Relative Capacity		Variation			Variation

1,000			293,131			44,470			559,780

10,000			308,090			36,730			424,130

20,000			310,651			36,220			421,620

30,000			312,768			42,380			506,220

Total			1,224,640		159,800			1,911,750

###### Allison C-4 Oxidation Test (J20C Spec.)

Tan Increase				7.0				7.0 max.

Carbonyl Absorbance			0.9				0.9 max.

Front Pump Seal				Moderate to 			Moderate to

Heavy Hardening			Heavy Hardening

Light Sludge			Light to Medium Sludge

Allison C-4 Wear Test

Total weight loss				1.4 mg				15.0 max.

Allison C-4 Paper Clutch Friction test

<=5,000   >5,000			<=5,000   >5,000

Cycles				Cycles

Slip Time, max.				0.70	0.55			0.72	0.61

Mid-Point Friction Coeff. min.		0.076	0.095			0.068	0.088

Allison C-4 Graphite Clutch Friction Test

1,500				5,500

Cycles

Slip Time, max.				0.70		0.74		0.71 max.

Mid-Point Friction Coeff. min.		0.101		0.097		0.104 min.

Biodegradability	CEC-L33A93		>80%

OECD 301B Mod. Sturm	>60%

ASTM D-5864		>60%

WGK Rating	1

Ecotoxicity

Fathead minnow, 96h LC50, 		>2000 ppm			EPA requirement >1000

Daphnia magna, 48h EC50,		>2000 ppm			EPA requirement >1000

Alga Growth Inhibition EC50	>2000 ppm			EPA requirement >1000

Meets EPA requirements 560/6-82-002, 560/6-82-003

Energy Conserving Formulation – USDA Biobased and BioPreferred