### Bio-E.P.™ 80W90 Gear Oil GL-4

# "Biobased Lubricants that Perform Like Synthetics"

Bio-E.P.™ 80W90 Gear Oil is designed to meet the GL-4 requirements of spiral bevel transmission and moderate service hypoid gears.  In industrial applications, it can be used as an Multi-Viscosity EP Gear Oil for lubricating spur, helical, bevel, and worm gear configurations where a multi-grade 80W90 can replace ISO 150 or 220 for cold temperature applications.  This formula has combined Stabilized HOBS technology with synthetic base stocks and mild EP/antiwear additives.  The result is an ultimately biodegradable1 product which has the long life heat stability but which additionally offers the protection advantages of increased gear life through extremely high film strength and excellent low temperature performance.  Bio-E.P.™ 80W90 Gear Oil is an ENVIRONMENTALLY RESPONSIBLE lubricant that is formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable material.

Typical Specifications

SAE Gear Grade				80W90

Specific Gravity @60OF (D-287)			0.92

VISCOSITIES:

@100OC., cSt. (D-445)			19.2

@40OC., cSt. (D-445)			121

Viscosity Index (D-2270)				180

Flash Point, COC, OC (D-92)			280

Pour Point, OC (D-97)				-30

Copper Corrosion Strip 3hr @ 100OC (D-130)	1A

4 Ball Wear, 1h, 167O F, 1200 RPM, 40kg (D-4172)	.30

FZG Test (DIN 51517)				>12

Demulsibility (D-2711)				Pass

Foam Sequence I, II, III (D-892)			Pass

Rust Prevention (D-665 A&B)			Pass

RLI Product Item #				82100

Features	(1) API Service Classifications GL-3, GL-4	and SAE 90

(2) Super high viscosity index and low pour point for wide temperature usage

(3) Fortified with additives to resist wear, oxidation, rust and foam

(4) Exceeds U.S. Steel and AGMA wear and EP performance

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA    1 Gallon  5 Gallon Pail   Drum    Totes     Bulk

RLI Item #				             82103        82104          82106     82107   82109