### Bio-Rock Drill™ Oils

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Rock Drill™ Oils are ultimately biodegradable1 vegetable oils formulated with Antiwear/EP, rust and oxidation inhibitors for the protection of pneumatic equipment. They are designed to emulsify water for improved lubricity in moist conditions and provide extra adhesiveness and anti-misting. Performance is enhanced by use of the Stabilized HOBS’s natural composition, which provides an oily boundary film.  The super high viscosity index of the Stabilized HOBS naturally improves the high temperature shear stability and fluid film strength between metal surfaces.  These (Bio Preferredsm,) products have shown to provide exceptional protection in equipment subject to extreme heavy shock loads and excessive moisture or water spray.  These biobased products have exceptional benefits over petroleum-based lubricants because there is direct danger of polluting the air, water, soil, or work environment through loss of the lubricant.

Bio-Rock Drill™ Oils meet the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  They exceed the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Rock Drill™ Oils are ENVIRONMENTALLY RESPONSIBLE lubricants that are formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable material.

1Ultimate/Readily Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Typical Specifications

ASTM		Medium		Heavy Medium	Heavy		Extreme Heavy

SAE Viscosity Grade				10W20		10W30		15W50		20W60

ISO Viscosity Grade				46		68		100		150

VISCOSITIES:			D-445

@100OC., cSt.					8.65		12.0		18.2		26.1

@40OC., cSt.					43.74		62.9		95		147

Viscosity Index			D-2270		181		191		212		213

Flash Point, COC,OC		D-92		260		272		288		290

Pour Point,OC			D-97		-36		-33		-30		-24

Copper Strip Corrosion (3h@100OC)	D-130		1A		1A		1A		1A

4-Ball Wear (mm)			D-4172		0.30		0.30		0.30		0.30

4-Ball EP				D-2783

Weld Point (kg)				250		250		250		250

Load Wear Index				47.86		47.86		47.86		47.86

Timken Load, OK Load (lbs)		D-2782		70		70		70		70

Rust Prevention			D-665

A-Distilled water			Pass		Pass		Pass		Pass

B-Syn. Sea water			Pass		Pass		Pass		Pass

RLI Product Item #				83000		83010		83020		83030

Applications

1.  Excellent recommendation for rock drills, jackhammers, and other pneumatic tools

2.  Also used as EP gear lubes (API GL-3), steam cylinder oils, way lubricants and non-drip oils

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.  Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA  1 Gallon   5 Gallon Pail    Drum  Totes  Bulk