### Bio-AW/AL™ Hydraulic Press Oils

### ISO 32, 46, 68

# "Biobased Lubricants that Perform Like Synthetics"

Bio-AW/AL™ Hydraulic Press Oils are ultimately biodegradable1 vegetable based formulas that replace mineral oil based hydraulic fluids in demanding press hydraulic systems.  Bio-AW/AL™ Hydraulic Press Oils are formulated to perform in hydraulic systems that require Anti-Wear (AW), Anti-Leak (AL), anti-rust, anti-oxidation, anti-foam, and demulsibility properties.  Bio-AW/AL™ Hydraulic Press Oils contain the same performance benefits and additive technology as the Bio-Ultimax™ 1000 Hydraulic Fluids with the addition of the anti-leak and/or non-drip performance.  They are highly inhibited against moisture and rusting in both fresh and sea water and pass A and B Sequences of the ASTM D-665 Turbine Oil Rust Test.  Incorporating the super high viscosity index of the Stabilized* High Oleic Base Stocks (HOBS) into the formula, increases the viscosity index past synthetic levels (Energy Conserving Formulas).  A zinc-free (ashless) additive system has also been developed that is environmentally friendly and meets or exceeds pump requirements.

Bio-AW/AL™ Hydraulic Press Oils are designed for use in mobile and stationary hydraulic vane, piston, and gear-type pumps when used in accordance with the equipment manufacturer.  Very little wear was encountered, 0 to 25mg (Pass), in accelerated biobased tests using Denison T-5D, Vickers 20VQ, 35VQ-25 (M-2950-S), and V-104C (ASTM D-2882) pump stand tests at pressures and temperatures ranging from 2000 to 3000 psi and from 1500 to 2100 F.  The anti-wear performance exceeds the load stage 10 in the FZG (DIN 51354) requirements for US Steel 136, DIN 51524 Part 2 and 3 (HLP/HVLP), and GM (LS-2).  They also meet the requirements for ashless GL-3 gear oils in reduction units and gear sets where they meet the viscosity ranges.

Bio-AW/AL™ Hydraulic Fluids meet the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used in hydraulic systems where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  They exceed the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Because they meet the environmental requirements they can also be used where ISO 15380 (HEES/HETG) Hydraulic Fluids are specified.  Bio-AW/AL™ Hydraulic Fluids are ENVIRONMENTALLY ACCEPTED LUBRICANTS (EALs) that are formulated from renewable biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants™* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants™, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B.: Hartville, Ohio, USA   1 Gallon    5 Gallon Pail    Drum  Totes  Bulk

Bio-AW/AL™ Hydraulic Press Oils ISO 32, 46, 68

The test data below show that the Bio-AW/AL™ Hydraulic Press Oils provide high performance in a wide variety of stationary and transportation equipment that operate in broad ranges of environmental conditions. In equipment operating outside, wear from poor cold temperature pumpability, surge loads, moisture, and dusty environments are more prominent.  Bio-AW/AL™ Hydraulic Press Oils are formulated to improve performance in equipment that requires excellent anti-wear, anti-leak, demulsibility, and cold temperature pumpability as low as -350C.

| TYPICAL SPECIFICATIONS | METHOD | ISO 32 | ISO 46 | ISO 68 | Spec. Requirements |
| --- | --- | --- | --- | --- | --- |
| Viscosity @ 40°C Viscosity @ 100°C Viscosity @ -15°C, Brookfield Viscosity @ -25°C, Brookfield Viscosity @ -30°C MRV TP1 Viscosity @ -35°C MRV TP1 Viscosity Index | ASTM D-445 ASTM D-445 ASTM D-2983 ASTM D-2983 ASTM D-4684 ASTM D-4684 ASTM D-2270 | 30.87 6.9 not complete 1,200 cP 4,500 cP 7,500 cP 184 | 43.8 9.67 1100 cP 3,000 cP 8,000 cP ----- 216 | 64.1 12.5 ----- ----- ----- ----- 198 | Note 1 Note 1 Note 1 Note 1 10W= <60,000 5W= <60,000 90 (min) |
| Pour Point Flash Point (COC) Fire Point (COC) Foam Sequence I, II, III (10 min) Rust Prevention Distilled Water Syn. Sea Water | ASTM D-97 ASTM D-92 ASTM D-92 ASTM D-892 ASTM D-665 | -40°C 236°C 260°C 0 Foam Pass Pass | -36°C 243°C 268°C 0 Foam Pass Pass | -30°C 251°C 274°C 0 Foam Pass Pass | Note 1 198°C (min) 218°C (min) 0 Foam Pass Pass |
| Copper Corrosion Strip 3hr @ 100°C | ASTM D-130 | 1B | 1B | 1B | DIN 51524 2(max) |
| Rotary Bomb Oxidation, (minutes) Oxidation Stability (Pressure Differential Scanning Calorimeter) min Neutralization Number mg KOH/g Swell of Synthetic NBR-L Rubber, % (Avg.) Volume Change (%) Shore A Hardness Change (%) Filterability A-No Water (s) (Avg) B-2% Water (s) (Avg) Demulsibility, ML Oil/Water/Emulsion 4-Ball Wear, 1h, 167°F, 1200 RPM, 40 kg FZG Test | ASTM D-2272 ASTM D-5483 Modified ASTM D-974 DIN 53538, Part 1 Denison TP 02100 HF-0 Requirement ASTM D-1401 ASTM D-4172 DIN 51354 | 360 70.0 (165°C) <0.4 6.0 -4 113 187 40/ 40/ 0 0.3 – 0.4 12 | 360 70.0 (165°C) <0.4 6.0 -4 268 271 40/ 40/ 0 0.3 – 0.4 12 | 360 70.0 (165°C) <0.4 6.0 -4 335 449 40/40/0 0.3 – 0.4 12 | USS 120 (min) Note 2 1.5 (max) 0 to 12 0 to -7 600 (max) 2xA (max) 40/37/3 (max) USS 127 0.5 (max) US.Steel 10 (min) |
| Biodegradation Classification Environmentally Friendly USDA Biobased Tested Environmental Management System Ecotoxicity LC-50 / EC-50 Note 1 Viscosity Sufficient for Application Note 2 Not Required | ASTM D-5864 OECD 301B ISO 15380 New Carbon ISO 14001 EPA 560/6-82-002, 003 | Ultimate PW1 Readily yes yes yes meets/exceeds | Ultimate PW1 Readily yes yes yes meets/exceeds | Ultimate PW1 Readily yes yes yes meets/exceeds | Ultimate PW1 Readily yes yes yes meets/exceeds |
| RLI Product Item # |  | 81410 | 81420 | 81430 |  |