### Bio-Chain & Cable™ Lubricants

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Chain & Cable™ Lubricants are ultimately biodegradable1 vegetable oils formulated with Antiwear/EP, rust/corrosion and oxidation inhibitors, and a tackifier.  Bio-Chain & Cable™ Lubricants are designed to provide multi-metal corrosion protection and recommended for heavy chains, sprockets, and cables, which are subject to heavy loading or shock loading.  These biobased products provide improved fire resistance over equal viscosity petroleum products and contain no chlorine, zinc, or heavy metals.  Performance is enhanced by use of the Stabilized HOBS’s natural vegetable oil composition, which provides an oily boundary film.  In addition, this oily film has a natural polarity to metal surfaces and helps clean and then penetrates deep into the inner core of the cable or chain link, preventing corrosion and wear.  The super high viscosity index of the Stabilized HOBS adds additional lubrication qualities to this high performance lubricant.  Laboratory and field tests have shown that the products provide exceptional equipment protection with excellent cold temperature pumpability.

Applications: Forestry, Mining, Marine, Agriculture, Heavy Industry, Rail and Shipping, Pulp and paper mills, saw mills, plywood mills, hoist cables and chains in marine shipping areas, draglines, drives on straddle lift lumber carriers, drip and automatic chain oilers, motorcycle and ATV chains, etc.  Field applications can be applied by spray, brush, dip, drip, or pressure boot.

Bio-Chain & Cable™ Lubricants meet the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  They exceed the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Chain & Cable™ Lubricants are ENVIRONMENTALLY RESPONSIBLE lubricants that are formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Typical Specifications

ASTM 		Medium		Heavy Med	Heavy		Extreme Heavy

ISO Viscosity Grade				46		68		100		150

SAE Viscosity Grade Replacement			10W20		10W30		15W50		20W60

VISCOSITIES:			D-445

@100OC., cSt.					8.65		12		18.2		26.1

@40OC., cSt.					43.74		62.9		95		147

Viscosity Index			D-2270		181		191		212		213

Flash Point, COC,OC		D-92		245		262		278		285

Pour Point,OC			D-97		-36		-33		-30		-26

Copper Strip Corrosion (3h@100OC)	D-130		1A		1A		1A		1A

4-Ball Wear (mm)			D-4172		0.30		0.30		0.30		0.30

4-Ball EP				D-2783

Weld Point (kg)				400		400		400		400

Load Wear Index				55		55		55		55

Timken Load, OK Load (lbs)		D-2782		70		70		70		70

Rust Prevention			D-665

A-Distilled water				Pass		Pass		Pass		Pass

B-Syn. Sea water				Pass		Pass		Pass		Pass

RLI Product Item #				83050		83060		83070		83080

STABILIZED by Renewable Lubricants™* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA     1 Gallon   5 Gallon Pail    Drum   Totes   Bulk