### Bio-Saw Guide™ Oils

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Saw Guide™ Oils are ultimately biodegradable1 vegetable oils formulated with Antiwear/Extreme Pressure additives, rust/corrosion and oxidation inhibitors, an emulsifier, and a tackifier.  They are specially formulated to lubricate modern “thin kerf” sawing systems.  Performance is enhanced by use of the Stabilized HOBS’s natural composition, which provides an oily boundary film.  The super high viscosity index of the Stabilized HOBS adds additional lubrication qualities to these high performance lubricants.  Bio-Saw Guide Oils can be used straight or their viscosity can be reduced with water.  Their emulsification helps in cleaning and dissolving pitch and allows correct mixing of oil and water.  In addition, they provide tackiness properties to allow the lubricant to cling to saw and guide components.

Applications: Bio-Saw Guide™ Oils meet or exceed the performance requirements of most saw system manufacturers including Kockums CanCar, CAE Newwes (McGehee), Optimill, Salem, TMT, Ukiah, and USNR (Schurman).

These biobased lubricants have exceptional benefits over petroleum-based lubricants because there is direct danger of polluting the air, water, soil, or work environment through loss of the lubricant.  Bio-Saw Guide Oils are ENVIRONMENTALLY RESPONSIBLE lubricants that are formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable material.

Typical Specifications

SAE ViscosityGrade Replacement			10W20		10W30		15W50		20W60

ISO Viscosity Grade				46		68		100		150

VISCOSITIES:			D-445

@100OC., cSt.					8.8		12.0		18.3		24.8.

@40OC., cSt.					44.6		63.3		95.9		141

Viscosity Index			D-2270		181		190		212		210

Flash Point, COC,OC		D-92		260		272		288		290

Pour Point,OC			D-97		-35		-33		-31		-24

Copper Strip Corrosion (3h@100OC)	D-130		1A		1A		1A		1A

4-Ball Wear (mm)			D-4172		0.30		0.30		0.30		0.30

4-Ball EP				D-2783

Weld Point (kg)				250		250		250		250

Load Wear Index				47.86		47.86		47.86		47.86

Timken Load, OK Load (lbs)		D-2782		70		70		70		70

Rust Prevention			D-665

A-Distilled water			Pass		Pass		Pass		Pass

B-Syn. Sea water			Pass		Pass		Pass		Pass

RLI Product Number				82500		82520		82540		82560

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA        1 Gallon    5 Gallon Pail    Drum   Totes   Bulk