### Bio-Arctic™ Firearm Lubricant

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Arctic™ Firearm Lubricant is a specially formulated ultimately biodegradable1 light lubricant that was developed to provide lubrication in a wide range of temperatures, with exceptional performance in extreme subzero temperatures.  The Stabilized* bio-synthetic base oils are formulated with the proper additive technology to lubricate into close tolerant areas and prevent corrosion.  In addition, this lubricant can help clean and prevent deposits from forming that cause weapons to jam.  The Bio-Arctic™ Firearm Lubricant provides very low temperature performance (pour point below -75OF), that prevents deposits from forming, firing pin misfires, and mechanism jamming.  The improved performance of Bio-Arctic Firearm Lubricant is a benefit in all firearms, but is especially noticeable with automatic weapon.  This improved performance will provide smoother mechanical action that is also noticeable in automatic weapons at temperatures above freezing.  It is a multi-functional high performance lubricant that can be used in many industrial applications.  Because of its biodegradability, this product has exceptional benefits over petroleum oils in these applications when there is direct loss of the lubricant into the water, soil, or work environment.

## Applications     - Military 	- Industrial	 - Transportation 	- Marine	 - Agricultural

Tools		Sports Equipment		Bearings			Bolts

Jacks		Assembly Parts		Wire ropes		Chains

Dies		Shafts			Hinges			Electronics

Locks		Linkage Cables 		Air Valves		Air Tools

## Typical Data

Viscosity   @ 40OC, cSt. 			ASTM D-445			9.7

Flash Point, PMCC				ASTM D-93			340OF (171OC)

Pour Point (Rotational)			ASTM D-5985			-54OC

Copper Corrosion Prevention			ASTM D-130			1A

Rust Prevention				ASTM D-665

Distilled Water							Pass-Clean

Synthetic Sea Water	Pass-Clean

Bio-Arctic™ Firearm Lubricant meets the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  It exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Arctic™ Firearm Lubricant is an ENVIRONMENTALLY RESPONSIBLE lubricant that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural biobased oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.   Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA	 Quart   1 Gallon    5 Gallon Pail    Drum    Totes    Bulk

RLI Product Item #				  81901	    81903		81904	        81906     81907    81909