### Bio-Asphalt ReleaseTM Agent

# "Biobased Lubricants that Perform Like Synthetics"

A specially formulated, ultimately biodegradable1 soy asphalt release agent that is a safe improvement over petroleum solvents for preventing asphalt from sticking and for cleaning tools and equipment.  This safe, nonflammable biobased product contains no hazardous Volatile Organic Compounds (VOCs).  It replaces diesel fuel and kerosene that are environmental problems and no longer accepted by EPA.   Bio-Asphalt Release ™ has exceptional benefits over petroleum oils in these applications because there is direct danger of polluting the water, soil, or work environment through loss of the petroleum lubricant.

The advantages are many:  biodegradable1, renewable, low toxicity, no hazardous VOCs, safer, OSHA and ISO 14000 compliant, reduces foreign oil and helps secure the American economy. EPA, OSHA and Workers Acceptance is high with Biobased Products.

Applications:

Truck Beds,  Chip and Seal Equipment,  Brooms,  Lutes,  Mauls,

Rollers,  Pavers,  Shovels,  Rakes,  Trawls,  Brushes

Directions:  May be used as a straight concentrate or may be solubilized with water before use to prevent build-up of asphalt, tar and oil.  Because the product is emulsifiable, it is more versatile and lower cost than diesel fuel when diluted 1 part of Bio-Asphalt ReleaseTM to 5 parts water.  Spray or brush truck beds and sides before hauling asphalt.  For best cleaning results, apply and let soak.  When used as a straight solution the product breaks down easily with a garden hose or pressure washer.  (Provides short term corrosion protection when used straight and can be diluted 1 part of Bio-Asphalt ReleaseTM with up to 10 parts water for some applications).

### TYPICAL TEST DATA:

ASTM D-445 9.0 cSt @ 40ºC				ASTM D-665-A Corrosion Protection- Pass

ASTM D-92 Flash Point 154 ºC				ASTM D-97 Pour Point -2.2oC

Pound Per Gallon   7.55					ASTM D-130 Copper Corrosion 1a

Emulsification with Water Yes

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Proprietary Formula

* Trademark of Renewable Lubricants, Inc.

Copyright 2002 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA	    1 Gallon    5 Gallon Pail    Drum   Totes   Bulk

RLI Product Item #				       86653	  86654             86656    86657   86659