### Bio-General Purpose™ Cut 30 & 40

(Cutting Oil and Machine Lube)

# "Biobased Lubricants that Perform Like Synthetics"

Bio-General Purpose™ Cut oils are ultimately biodegradable1, biobased lubricants for light to medium duty machining operations.  Their color can be classified as transparent, which permits viewing the cutting operations while in process and they are formulated to reduce smoke and mist.  Performance is enhanced by use of the Stabilized HOBS’s, natural fatty acid composition, which provides cutting tool wetting and oiliness; combined with excellent extreme pressure and antiwear technology.  The super high viscosity index of the Stabilized HOBS adds additional load carrying properties in machining application.  They are non-staining to yellow metals and may be used for machining both ferrous and non-ferrous metal alloys.  These (Biopreferredsm,) products do not contain active sulfur, chlorine, zinc, phosphorus, silicon, or heavy metals, and do not produce an abrasive odor.  Bio-General Purpose Cut oils extreme pressure properties can be increased by the addition of Bio-Syntra™ and Bio-SynXtra™ MW Oils (see data sheets for Bio-Syntra™ and Bio-SynXtra™ products).  The flexibility of these products helps in reducing inventory and lowering cost.

The advantages are many:  biodegradable, renewable, low toxicity, no hazardous volatile organic compounds (VOC), more fire resistant, safer, EPA and ISO 14000 compliant, reduces foreign oil, and helps secure the American Economy, OSHA and worker acceptance is high with biobased oils.

Bio-General Purpose™ oils are ENVIRONMENTALLY RESPONSIBLE lubricants that are formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable materials.

Typical Specifications

Grade							30		40

Specific Gravity @60OF.				.89		.90

VISCOSITIES:@  100OC., cSt.				7.0		9.0

@40OC., cSt.				29.2		40.0

Viscosity Index						215		216

Flash Point, COC OC					218		240

Pour Point, OC						-16		-18

Copper Corrosion ASTM D-130				1B		1B

Rust Prevention ASTM D-665				No Rust	No Rust

4-Ball Wear ASTM D-4172 (mm)			.40		.35

4-Ball EP Weld Pt. ASTM D-2783 (kg)			250		315

Load Wear Index				36		41

RLI Product Item #					86820		86830

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454, Patent 6,624,124, US Patent 6,620,772 with additional Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA        1 Gallon    5 Gallon Pail    Drum    Bulk