### Bio-SynXtra™ Super Viscosity EHD-MW

(Super Viscosity Extra Heavy-Duty Metal Working Oils)

# "Biobased Lubricants that Perform Like Synthetics"

Bio-SynXtra™ Super Viscosity EHD-MW oils are biodegradable1, biobased metal working oils formulated from Super High Viscosity natural and synthetic esters for extra heavy-duty metal working operations.  Their color can be classified as transparent, which permits viewing the cutting operations while in process and they are formulated to reduce smoke and mist.  Performance is enhanced by use of the Stabilized HOBS’s, natural fatty acid composition, which provides tool wetting and oiliness; combined with exceptional extreme pressure (EP) antiwear technology and corrosion protection.  The super high viscosity index of the Stabilized HOBS and synthetic base stocks adds additional load carrying properties for deep drawing, and cold heading applications.

These (Biopreferredsm,) products do not contain active sulfur, chlorine, zinc, phosphorus, silicon, or heavy metals, and do not produce an abrasive odor.  They are non-staining to yellow metals and may be used for machining both ferrous and non-ferrous metal alloys.  These operations include: Extra Heavy Duty and/or low speed stamping, drawing, milling, drilling, turning, grinding, shaving, sawing, broaching, thread cutting, and tapping.  In addition, these oils are particularly useful for working stainless and hard steel, such as Hastalloy and tool steels.  More specific Extra Heavy-Duty applications include steel and stainless steel wire drawing, deep drawing, and cold heading (match heavy viscosities and EP performance below to equipment and application requirements).

The advantages are many:  biodegradable, renewable, low toxicity, no hazardous volatile organic compounds (VOC), more fire resistant, safer, EPA and ISO 14000 compliant, reduces foreign oil, and helps secure the American Economy, OSHA and worker acceptance is high with biobased oils.

Bio-SynXtra™ Super Viscosity EHD-MW oils are ENVIRONMENTALLY RESPONSIBLE lubricants that are formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable materials.

Typical Specifications

ISO Grades			   		150	  		220			460

Specific Gravity  @60OF.				.95			 .96			.96

VISCOSITIES:@100OC., cSt.			25			35			60

@40OC., cSt.			143			211			430

Viscosity Index					210			215			212

Flash Point, COC OC				290			290			290

Pour Point, OC					-12			-10			-4

Copper Corrosion ASTM D-130			1B			1B			1B

Rust Prevention ASTM D-665 A&B		No Rust			No Rust			No Rust

4-Ball EP Weld Pt. ASTM D-2783 (kg)		>800			>800			>800

Product Item #					88170			88180			88190

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1Inherently or Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454, with additional Pending and Foreign Patents

*Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability  F.O.B. :Hartville, Ohio, USA     1 Gallon   5 Gallon Pail    Drum    Totes    Bulk