### Bio-Heavy Duty™ Cutting Oil

# "Biobased Lubricants that Perform Like Synthetics"

A heavy duty, ultimately biodegradable1, vegetable based, cutting oil which provides excellent performance in a wide variety of machining operations on tough ferrous alloys as well as mild steel and cast iron.  These operations include: milling, drilling, turning, grinding, light and medium duty broaching, and thread cutting and tapping.  This product replaces the use of products that contain chlorinated paraffin additives.

Performance is enhanced by use of the Stabilized HOBS’s, natural fatty acid composition, which provides cutting tool wetting and oiliness; combined with sulfur/phosphorous EP and antiwear technology.  The super high viscosity index of the Stabilized HOBS adds additional lubrication qualities to this high performance lubricant.

Bio-Heavy Duty™ Cutting Oil is an ENVIRONMENTALLY RESPONSIBLE cutting oil that is formulated from renewable agricultural plant resources.  We believe Earth’s environmental future rests in the use of renewable materials.

Typical  Specifications

SAE Grade						30

ISO Grade						46

Pounds/Gallon @ 60OF.					7.39

Specific Gravity @60OF.				0.887

VISCOSITIES:

@100OC., cSt.					9.63

@40OC., cSt.					45.7

Viscosity Index						202

Flash Point, COC, OC.					250

Pour Point, OC.						-18

Copper Corrosion ASTM D-130				1-B

Rust Prevention ASTM D-665

A (Distilled Water)				No Rust

B (Synthetic Sea Water)				No Rust

Tapping Test

304 Stainless Steel, % Efficiency		125

1020 HR Steel, % Efficiency			120

Falex EP Test, (Fail load lbs.)			4250

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils. This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA      1 Gallon   5 Gallon Pail   Drum    Totes   Bulk

RLI Product Item #				             86713	        86714	   86716      86717     86719