### Bio-Mist™ EP Cutting Oil

# "Biobased Lubricants that Perform Like Synthetics"

A heavy duty, ultimately biodegradable1, vegetable based, mist EP cutting oil which provides excellent performance  where misting or on standard cutting applications are needed in a wide variety of machining operations non-ferrous metals, tough ferrous alloys as well as mild steel and cast iron.  These operations include: milling, drilling, turning, grinding, broaching, and thread cutting and tapping.  This (Biopreferredsm product does not contain active sulfur, chlorine, zinc, phosphorus, silicon, or heavy metals, and does not produce an abrasive odor and is non-staining.  In addition, this oil is particularly useful for machining stainless and harder materials, such as tool steels, Inconel, and Hastalloy.

Performance is enhanced by use of the Stabilized HOBS’s, natural ester composition, which provides cutting tool wetting and oiliness; combined with EP and antiwear components.  The super high viscosity index of the Stabilized™ HOBS adds additional cutting qualities to this high performance lubricant.

The advantages are many:  biobased, biodegradable, renewable, low toxicity, no hazardous volatile organic compounds (VOC), more fire resistant, safer, EPA and ISO 14000 compliant, reduces foreign oil, and helps secure the American Economy, OSHA and worker acceptance is high with biobased oils.

Typical  Specifications

ISO Grade						32

VISCOSITIES:

@100 OF SUS					145

@40OC., cSt.					31.3

@100OC., cSt.					7.3

Viscosity Index						211

Flash Point, COC,.					204 OC	(400 OF)

Pour Point, OC.						-14

Copper Corrosion ASTM D-130				1B

4-Ball EP ASTM D-2783

Non-Seizure Load kg				126

Weld Load kg					800

Load Wear Index					152

Rust Prevention ASTM D-665				No Rust

Tapping Test

304 Stainless Steel, % Efficiency			125

1020 HR Steel, % Efficiency			120

Falex EP Test, (Fail load lbs.)			4250

Bio-Mist™ EP Cutting Oil meets the Environmental Protection Agency (EPA) Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used in applications where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  It exceeds the acute toxicity (LC-50 / EC-50 >1000 ppm) criteria adopted by the US Fish and Wildlife Service and the US EPA.  Bio-Mist™ EP Cutting Oil is an ENVIRONMENTALLY ACCEPTED LUBRICANT that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils. This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454, US Patent 6,624,124, US Patent 6,620,772 with additional Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B.: Hartville, Ohio, USA    1 Gallon   5 Gallon Pail    Drum  Totes   Bulk

RLI Product Item # 				          86733	      86734               86736    86737    86739