### Bio-SynXtra EP Open Gear Grease

# "Biobased Lubricants that Perform Like Synthetics"

PRODUCT BENEFITS

  - Biodegradable, Tacky/adhesive, High viscosity (>1800 cSt @ 40°C).

  - Capable of handling heavy loads at slow speeds and performing in a wet environment where exposure to rain is possible. Can be sprayed - or - diluted in a suitable solvent to allow it to be sprayed.

| Test Method | Test | Biodegradable Open Gear Grease |
| --- | --- | --- |
| Visual | Color | Black |
| Visual | Appearance/texture | Smooth/Very tacky |
|  | Base Oil viscosity, cSt: |  |
| D445 | 40°C | 1908 |
| D445 | 100°C | 227.4 |
| D2270 | VI | 258 |
|  | Base oil type | Synthetic/Natural esters |
| D217 | Penetration, unworked | 325 |
| D217 | Penetration, Worked, 60X | 325 |
| D2596 | 4 ball weld (kg) | 620 |
| D2266 | 4 ball wear, scar diameter | 0.66 mm |
|  | Coefficient of Friction | 0.058 |
| D4049 | Water Sprayoff, % loss | 2.9 |
| D4048 | Copper Corrosion, rating | 1b |
| CTM-1 | Evaporation Loss, % loss | 0.25 |
| D1743 | Rust Test, DI water | Pass |
| D1831 | Dry Roll Stability, 2hrs @ 25°C | 9.26% |
| D1831 | Wet Roll Stability, 10% water, 2hrs @ 25°C | 15.12% |
| CTM-3 | Brookfield Viscosity, T-C spindle, 1 rpm |  |
|  | 0°C | 1,192,000 cP |
|  | -10°C | 1,968,000 cP |
|  | -20°C | 6,960,000 cP |
|  | Lincoln Ventmeter, psi @ |  |
|  | 0°C/32°F | 320 psi |
|  | -10°C/14°F | 650 psi |
|  | -20°C/-4°F | 1180 psi |

Bio-SynXtra EP Open Gear Grease meets the Environmental Protection Agency (EPA) 2013 Vessel General Permit (VGP) guidelines for Environmentally Acceptable Lubricants (EALs), and should be used where LOW TOXICITY, BIODEGRADABILITY and NON-BIOACCUMULATION properties are required.  Bio-SynXtra EP Open Gear Grease is an ENVIRONMENTALLY RESPONSIBLE lubricant that is formulated from renewable agricultural biobased resources.  We believe Earth's environmental future rests in the use of renewable materials.

1Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricants.  Readily Biodegradable within OECD 301B Method

STABILIZED by Renewable Lubricants™* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high-performance formula in high and low temperature applications, reducing oil thickening and deposits.

Patented Product: US Patent 6,383,992, US Patent 6,534,454 with additional Pending and Foreign Patents

™ Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B.: Hartville, Ohio, USA      5 Gal Pail   Drum   Totes   Bulk

Item # NLGI #1 Biobased Open Gear Grease