### BPL™ Food Grade Plus Tack (H1)

# "Biobased Lubricants that Perform Like Synthetics"

BPL™ Food Grade Plus Tack is a specially formulated, biodegradable, biobased penetrant that can be used as a light tacky lubricant in food processing equipment and is essentially odorless and tasteless.  Because of the super high viscosity index of the Stabilized* HOBS, this product performs in many applications.  BPL™’s patented composition of additives and base fluids provides a protective, tacky thin film lubricant.  This natural oily film has shown in laboratory and field tests to out perform petroleum base oils in terms of natural lubricity.

BPL™ Food Grade1 Plus Tack is formulated to penetrate into close tolerant areas, then lubricate, and prevent corrosion.  BPL™’s ability to creep is demonstrated by placing a 3/8” x 2” bolt on its head with ¼” of BPL™ in the bottom of a lab beaker; BPL™ creeps vertically up the threads.  It protects deep into the core of a cable or chain link and is excellent as a light air tool lubricant and preservative oil for parts.  This Biobased product has exceptional benefits over petroleum oils in these applications because there is direct danger of polluting the water, soil, or work environment through loss of the lubricant.  BPL™ contains no hazardous volatile organic compounds (VOCs). EPA, OHSA, and Workers Acceptance is  high with Biobased Products. Contains no animal byproducts and are manufactured under kosher supervision.

## Applications With Incidental Food Contact In and Around Food Processing Equipment Areas

## - Military 	- Industrial	 - Transportation 	- Marine	 - Agricultural

Tools		Gaskets/Seals		Bearings		Bolts

Jacks		Assembly Parts		Wire ropes		Chains

Dies		Machine Tools		Hinges			Shafts

Locks		Linkage Cables 		Air Valves		Air Tools

NSF Registration:							140448 H1, H2

140450 H1, H2 -Aerosol

Typical Data

Specific Gravity @60OF.			ASTM D-287			.88

Viscosity @40OC., cSt.			ASTM D-445			14

Flash Point, PMCC			ASTM D-93			295OF (146OC)

Pour Point 				ASTM D-97			-25OC

Copper Corrosion Prevention		ASTM D-130			1A

Rust Prevention				ASTM D-665

Distilled Water							Pass-Clean

Synthetic Sea Water	Pass-Clean

Four Ball Wear				ASTM D-2266	.40 mm

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented  technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 This product is acceptable as a lubricant with incidental food contact (H1) for use in and around food processing areas. Such compounds may be used on food processing equipment as a protective anti-rust film, as a release agent on gaskets or seals of tank closures, and as a lubricant for machine parts and equipment in locations in which there is a potential exposure of the lubricated part to food.

Patented Product: US Patent 6,383,992, US Patent 6,534,454, US Patent 6,624,124, US Patent 6,620,772 with additional Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA	 8oz. Spray   1 Gallon      5 Gallon Pails    Drums    Bulk

RLI Product Item #