### Bio-SynXtra HFC Refrigeration Compressor Lubricant

(ISO 68)

Bio-SynXtra HFC Refrigeration Compressor Lubricant is a formulated ISO 68 grade synthetic polyol ester refrigeration lubricant specifically designed to be compatible and provide top tier performance with systems using ozone-friendly, chlorine-free HFC refrigerants.  Bio-SynXtra HFC provides exceptional high temperature stability, wear protection, and longer service life in refrigeration and air conditioning systems that require HFC (hydrofluorocarbon) refrigerants R-134a, R-404A, R-407C and R-410A and with R-22 retrofit blends such as R-417A, R-422A, R-422D, and R-427.

Bio-SynXtra HFC is highly recommended for newer generation energy efficient and environmentally friendly refrigerants technologies, including R-32, CO2, HCs, HFOs and their blends.  It provided excellent low temperature fluidity, no waxy deposits, improved evaporator efficiency, and can meet specific viscosity requirements of a wide range of equipment and applications.

Multi-Applications:  Reciprocating, rotary, scroll, centrifugal/screw refrigeration compressors, and recommended for carbon dioxide applications with appropriate miscibility for proper oil return to compressor (typically piston type applications).  In addition, the product is compatible and recommended for CFC (chlorofluorocarbon) and HCFC (hydro- chlorofluorocarbon) refrigerants.

Compatible with HCFC, CFC, & HFC refrigerants

| TYPICAL SPECIFICTION | ISO 68 | METHOD |
| --- | --- | --- |
| Appearance | Clear and Bright Liquid | Visual |
| Kinematic Viscosity @ 100 ºC, cSt | 8.76 | ASTM D-445 |
| @ 40 ºC, cSt | 66.5 | ASTM D-445 |
| Viscosity Index | 104 | ASTM D-2270 |
| Total Acid Number, mg KOH/g | 0.02 | ASTM D-974 mod |
| Pour Point, °C | -40 | ASTM D-92 |
| Flash Point, °C | 260 | ASTM D-5950 |
| Specific Gravity, 15.6 ºC/15.6 ºC | 0.965 | ASTM D-4052 |
| Density @ 15.6 ºC, lbs/gal | 8.04 | ASTM D-4052 |
| Water, ppm | 50 max | ASTM D-1533 |
| Low Temperature Miscibility Limit (10 Vol % lubricant in refrigerant, ºC) |  | Sealed Tube |
| R-134a | <-35 |  |
| R-404A | <-60 |  |
| R-407C | <-35 |  |
| R-410A | <-30 |  |
| RLI Product Item # | 87820 |  |

™Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability F.O.B.: Hartville, Ohio, USA 	1 Gallon 		Drum 	Totes	Bulk

87823		87826	87827	87829