### Bio-Food Grade™ Cutting Oils  (H1)

(Cutting Oils and Machine Lubes)

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Food Grade™ Cutting Oils are biobased food grade1 lubricants for light to medium duty machining operations. The color can be classified as transparent, which permits viewing the cutting operations while in process and it is formulated to reduce smoke and mist. Performance is enhanced by use of the Stabilized HOBS’s, natural fatty acid composition, which provides cutting tool wetting and oiliness; combined with excellent extreme pressure and antiwear technology. The super high viscosity index of the Stabilized HOBS adds additional load carrying properties in machining application. They are non-staining to aluminum and yellow metals, and may be used for machining both ferrous and non-ferrous metal alloys. These (BioPreferredsm) products do not contain active sulfur, chlorine, zinc, or heavy metals, and do not produce an abrasive odor.

The advantages are many:  biodegradable, renewable, low toxicity, no hazardous volatile organic compounds (VOC), more fire resistant, safer, EPA and ISO 14000 compliant, reduces foreign oil, and helps secure the American Economy. OSHA and worker acceptance is high with biobased oils. Contains no animal byproducts and are manufactured under kosher supervision.

They are ENVIRONMENTALLY RESPONSIBLE lubricants formulated from renewable agricultural plant resources. Earth’s environmental future rests in the use of renewable materials.

Typical Specifications

ISO Grade					32		46		68

Specific Gravity @60OF.			.88		.89		.89

VISCOSITIES:@  100OC., cSt.			7.0		9.3		13.3

@40OC., cSt.			31.6		45.0		65.4

Viscosity Index					193		196		210

Flash Point, COC OC				230		241		249

Pour Point, OC					-35		-30		-25

Copper Corrosion ASTM D-130			1A		1A		1A

Rust Prevention ASTM D-665			No Rust	No Rust	No Rust

4-Ball Wear ASTM D-4172 (mm)		.35		.35		.35

4-Ball EP Weld Pt. ASTM D-2783 (kg)		200		200		200

Load Wear Index			47		47		47

RLI Product Item #					88330		88340		88350

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented anti-oxidant, anti-wear, and cold flow technology. High Oleic Base Stock (HOBS) are agricultural vegetable oils. This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1 Base oils and additives in this product are listed in 21 CFR 178.3570, Lubricants for incidental food contact (USDA H1).

Full compliance with other applicable restrictions of FDA, USDA, oil spill, and oil pollution prevention statutes is recommended.

Patented Product with Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.  Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Hartville, Ohio, USA      1 Gallon   5 Gallon Pail   Drum   Totes   Bulk