### Bio-SynXtra™ High Temperature Lubricants

### ISO 68, 100, 150, 220    (Food Grade H1)

# "Biobased Lubricants that Perform Like Synthetics"

Bio-SynXtra™ High Temperature Lubricants are unique biobased, saturated synthetic-ester, food grade1 lubricants designed to lubricate bearings, chains, slides, and gears in industrial applications where air temperatures often exceed 500ºF (260ºC).  These biodegradable2 products are free of Volatile Organic Compounds (VOCs), provide very high fire points (ASTM D-92), and contain No Petroleum Carbon.

High Temperature Applications:

-Roller chains on oven conveyors

-Lithographic chains, beverage can lines

-Tenter frames in textile plants

-Kiln car wheel bearing/refractory plants

-Paint lines, drying ovens

-Sealed for life units

-Kiln support rollers, cement plants

-Bakery oven chains

-Automatic lubrication systems

-Heat transfer fluids

Multi-Applications: Hydraulic systems, compressors, gear drives, gearhead motors, drip oilers, air-tools, water pumps, bearings, machine oils, chains, cables, turbines, circulating oils, etc., and general high temperature lubrication.

Outstanding Advantages:

Exceptional High Temperature Stability- made from bio-synthetic and biodegradable2 base oils that reduce tendency to form hard carbon deposits in high temperature applications up to 270ºC.

Cleanliness (ashless) - helps to eliminate accumulation of hard carbon solids that create maintenance clean-up problems and downtime, cleans chains already dirtied by inferior lubricants.

Better Protection- reduces wear, rust, oxidation, and corrosion; extends equipment life, reduces maintenance costs.

Low Volatility- maintains a liquid lubricating film at elevated temperatures, thus providing substantially longer lubrication intervals, reduced lubricant consumption, less smoke, and no bad odors.

Energy Efficient- clean, fluid-film lubricants, reduce energy consumption in equipment.

Optimum Viscosity- is provided by the High Viscosity Index that gives optimum lubrication at higher operating temperatures.

Eco-Non Toxic- complies with Environmental Management System ISO 14001 and Environmentally Friendly ISO15380

1Base oils and additives in these products are listed in 21 CFR 178.3570, NSF HX-1 food grade components, and Lubricants for incidental food contact (USDA H1). Full compliance with other applicable restrictions of FDA, USDA, oil spill, and oil pollution prevention statutes is recommended.

2Ultimate Biodegradation (Pw1) within 28 days in ASTM D-5864 Aerobic Aquatic Biodegradation of Lubricant

* Trademark of Renewable Lubricants, Inc.               Copyright 2012 Renewable Lubricants, Inc

Availability	F.O.B. :Hartville, Ohio, USA     1 Gallon    5 Gallon Pail    Drum    Totes    Bulk

Elastomer Compatibility: Bio-SynXtra™ High Temperature Lubricants are recommended for uses with fluorocarbon (Viton), fluorosilicone, polysulfide and high nitrile Buna-N (>30%) elastomers.

Bio-SynXtra™ High Temperature Lubricants are not recommended for use where neoprene, natural rubber, styrene-butadiene rubber (SBR, Buna S) or low Buna-N seals are used.

Typical Specifications for Bio-SynXtra™ High Temperature Lubricants (H-1)

| ISO Grade | 68 | 100 | 150 | 220 |
| --- | --- | --- | --- | --- |
| Specific Gravity @ 60°F, (ASTM D-287) | .98 | .98 | .99 | 1.0 |
| Viscosity (ASTM D-445) @100°C cSt @40°C cSt | 10.0 64.0 | 13.9 99.0 | 17.8 137.0 | 24.0 205 |
| Viscosity Index (ASTM D-2270) | 141 | 142 | 144 | 145 |
| NOACK Volatility %, 250°C (ASTM D-5800) | 2.5 | 2.5 | 2.0 | 2.0 |
| Evaporation Loss, Wt %, 6.5 hrs, 250°C (ASTM D-972) | 3.0 | 3.0 | 2.9 | 2.9 |
| Flash Point (ASTM D-92) | 265°C | 268°C | 270°C | 270°C |
| Fire Point, COC (ASTM D-92) | 304°C | 309°C | 309°C | 309°C |
| Pour Point (ASTM D-97) | -48°C | -45°C | -43°C | -40°C |
| Foam Sequence I, II, III (D-892) | 0 Foam | 0 Foam | 0 Foam | 0 Foam |
| Rust Prevention A,B (ASTM D-665) | Pass | Pass | Pass | Pass |
| Copper Corrosion Strip 3hr @ 100°C (ASTM D-130) | 1A | 1A | 1A | 1A |
| 4 Ball Wear,1h, 54°C ,1800 RPM, 20kg (U.S. Steel S-205) | 0.35 mm | 0.32 mm | 0.32 mm | 0.32 mm |
| 4 Ball Weld (ASTM D-2783) Load Wear Index | 200kg 46 | 200kg 47 | 200kg 47 | 200kg 47 |
| FZG Test (DIN 51354) | 12 | 12 | 12 | 12 |
| Product Item # | 81810 | 81820 | 81830 | 81840 |

Bio-SynXtra™ High Temperature Lubricants are ENVIRONMENTALLY RESPONSIBLE products that are formulated from renewable agricultural resources.  We believe Earth's environmental future rests in the use of renewable materials.