Bio-Food Grade™ E.P. Grease

### NLGI # 0, # 1, #2 (High Temperature) H1

# "Biobased Lubricants that Perform Like Synthetics"

Bio-Food Grade™1 E.P. Greases are high temperature Biobased greases with excellent E.P. and Antiwear performance.  The super high viscosity index of the Stabilized* HOBS naturally improves the thermal shear stability and load capacity.  They were engineered specifically for food processing and packaging machinery.  Bio-Food Grade™ E.P. Greases are rust and oxidation inhibited formulas that are very resistant to water and maybe used as open or enclosed gear greases.  These products provide superior high temperature performance and good adhesion/cohesion properties.  They have a neutral odor and are non-staining.  The # 1 & # 0 are Supreme High Temperature Food Grade Grease with improved cold temperature mobility over Bio-Food Grade™ E.P. NLGI #2.  Bio Food Grade™ E.P. Grease contains an optimized blend of preservatives. The preservatives exhibit broad spectrum antimicrobial activity against Gram positive and Gram negative bacteria, yeasts and mold. Meets and exceeds outdated military specification for Food Grade Grease DOD-G-24650. Contains no animal byproducts and are manufactured under kosher supervision.

NLGI # 1		NLGI # 0		NLGI # 2

NSF Registration:				140452 H1		140451 H1		140453 H1

Typical Specifications:

Base Oil -Viscosity @ 40○C cSt ASTM D 445	42.10			42.10			42.10

Viscosity @ 100○C cSt ASTM D 445	8.69			8.69			8.69

Viscosity Index ASTM D 2270		191			191			191

Pour Point ASTM D 97			-30○C			-30○C			-30○C

Color					White			White			White

Thickener				Alum Complex		Alum Complex		Alum Complex

Drop Point ASTM D 566				5000 F (260o C)		NA			5270 F (275o C)

Water Washout @ 790 C ASTM D 1264		3.4 % Loss		NA			2.0% Loss

Mobility Test-US Steel Method

40oC											217.00 g/min

0 oC											13 g/min

-20oC											2.6g/min

4-Ball Wear ASTM D 2266			0.46 mm			0.46 mm			0.43 mm

4-Ball EP ASTM D 2596				Weld 250		Weld 250		Weld 315

Timken OK Load ASTM D 2509.			40 lbs.			40 lbs.			40 lbs.

Pen, Unwkd ASTM D 217				325 mm/10		380 mm/10		286 mm/10

Pen, Wkd 60 ASTM D 217 		320 mm/10		390 mm/10		295 mm/10

Pen, Wkd 10,000				340 mm/10		390 mm/10		304 mm/10

Pen, Wkd 100,000			340 mm/10		390 mm/10		293 mm/10

ASTM D 217 strokes change from 60 strokes

Roll Stability ASTM D 1831			-3.5%			385%			+3.0%

Cone Bleed @ 1000 C ASTM D 6184		3.7 % Loss		NA			1.9 % Loss

Copper Corrosion ASTM D 130			1A			1A			1B

Oil Separation ASTM D 1742			4.6 % Loss		NA			1.1 % Loss

Rust Test ASTM D 1743				Pass			Pass			Pass

Bomb Oxidation, 100 h. ASTM D 942		5.0 psi			5.0 psi			3.0 psi

RLI Product Item #				87510			87520			87500

STABILIZED by Renewable Lubricants* is RLI’s trademark on their proprietary and patented technology.  High Oleic Base Stock (HOBS) are agricultural vegetable oils.  This Stabilized technology allows the HOBS to perform as a high performance formula in high and low temperature applications, reducing oil thickening and deposits.

1This product is acceptable as a lubricant with incidental food contact (H1) for use in and around food processing areas. Such compounds may be used on food processing equipment as a protective anti-rust film, as a release agent on gaskets or seals of tank closures, and as a lubricant for machine parts and equipment in locations in which there is a potential exposure of the lubricated part to food.

Patented Product with Pending and Foreign Patents

* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Manufacturer	    14 oz. Tube    35 lb  Pail    120 lb Keg    400 lb Drum

(8,000 Pound Minimum Batches)