RLI Heavy Synthetic Food Grade (H1) Grease

### NLGI 2, (High Temperature)

RLI Heavy Synthetic Food Grade (H1) Grease (NLGI 2) is a food grade1 aluminum complex thickened lubricating grease with a heavy synthetic base oil. It is formulated specifically for the food packaging and processing industry, water treatment, and in other environmental areas were this lubricant may have incidental contact in the application. RLI Heavy Synthetic Food Grade (H1) Grease provides excellent extreme pressure and antiwear protection and can be used over a wide range of operating temperatures. This product provides excellent lubrication in heavy loaded/slower moving bearings were a 220 cSt base oil gives additional protection. Contains no animal byproducts and are manufactured under kosher supervision.

Typical Specifications:

NLGI Grade 								2

Soap Type								Aluminum Complex

Texture									Smooth, Adhesive

Color									White

Worked Penetration, ASTM D 217,

60 strokes							265-295

Dropping Point, ASTM D 2265, 0F 						500 min.

Rust & Corrosion, ASTM D 1743						Pass

Base Oil Viscosity with polymer

cSt @ 400C,							190-240

cSt @ 1000C,							18.6Min

Viscosity Index

Flash Point, °F (°C)							430(221)

Pour Point, 0 F (C)	-							-10

Timken OK Load Lbs. ASTM D 2509						40

Four Ball Wear, ASTM D 2266 Scar diameter, mm.				0.60

Four Ball EP, Weld Point, ASTM D 2596 Kgf					500

Copper Corrosion, ASTM D 4048						1b

Water Washout, ASTM D 1264

1 hr, 0 F, % Loss							5

Roll Stability, ASTM D 1831

2 Hrs,0 F, % Change						10 max

Oxidation Stability, ASTM D 942

PSI drop 100 hours							5 max

PSI drop 500 hours								10 max

1 Base oils and additives in this product are listed in 21 CFR 178.3570, Lubricants for incidental food contact (USDA H1).  Full compliance with other applicable restrictions of FDA, USDA, oil spill, and oil pollution prevention statutes is recommended. This product is acceptable as a lubricant with incidental food contact (H1) for use in and around food processing areas. Such compounds may be used on food processing equipment as a protective anti-rust film, as a release agent on gaskets or seals of tank closures, and as a lubricant for machine parts and equipment in locations in which there is a potential exposure of the lubricated part to food.

Proprietary Formula

* Trademark of Renewable Lubricants, Inc.   Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Manufacturer	14oz Tube	35 lb  Pail    120 lb Keg    400 lb Drum

RLI Product Item #				   87491	   87494 	87495		87496