### MaxxLife™ Food Grade H1 Multipurpose Grease

NLGI # 2

This Food Grade EP grease is a state-of-the-art product, characterized by excellent resistance to water and superior corrosion protection.  The exceptional mechanical and oxidation stability, and outstanding performance in a wide temperature range, make this product a premium multipurpose grease.  In addition, it is formulated with a state-of-the-art overbased calcium sulfonate thickener that gives long life at high temperatures with high extreme pressure characteristics.  It contains no zinc, heavy metals or other harmful or environmentally undesirable additives. Meets and Exceeds old Military specification for Food Grade Grease DOD-G-24650. Contains no animal byproducts and are manufactured under kosher supervision.

Applications:  Food processing equipment as a protective anti-rust film, release agent on gaskets or seals of tank enclosures, anti-seize and/or lubricant for machine parts and equipment that may come in contact in part to food, including conveyors, antifriction and journal bearings, electric motors, and pumps can benefit from its long lasting protection.

- Unique multipurpose food grade industrial grease

- Excellent low temperature properties

- Superior corrosion protection

- Environmentally friendly

- Excellent compatibility with other greases

Typical Specifications:					ASTM

Penetration 						D-217

Worked 60 strokes								265-295

Unworked 								265-295

Worked 100,000 Stokes Penetration Change, FTM 791 C 313.2			+/-5%

Base Oil Characteristics 					D-445

Viscosity	@ 40 oC cST  							100

Viscosity	@ 100 oC cST  							10.8

Viscosity Index  						D-2270		90

Pour Point 						D-97		-12 oC

Flash Point 						D-92		220 oC

Dropping Point , oF (oC)					D-2265		+572 (+300)

Water Washout @ 175oF (79 oC), % loss 			D-1264		2.75

4-Ball Wear test 40kg, 1200 RPM,75 oC, mm Scar Diameter 	D-2266		0.45 Max

4-Ball E.P. Weld point, kgf					D-2596		620

Timken, 0 K load, Lbs  					D-2509		  65

Salt Fog Test, B-117 Hrs. 					B-117		+2,500

Oxidation Stability, 100 hours @ 99 oC	 			D-942		1 psi (7kPa)

Wheel Bearing, grams @ 325oF (163 oC) 			D-1263		0.4

Copper Strip Corrosion  					D-4048		1a

Corrosion Preventative Properties 			D1743	D-1478		Pass

Low Temperature Torque, -40 oF (-40 oC),gram-cm 		D-1478		<5,000

Oil Separation 						D-1742   		0.2%

* Trademark of Renewable Lubricants, Inc.

Copyright 2012 Renewable Lubricants, Inc.

Availability	F.O.B. :Manufacturer	 14 oz. Tube    35 lb  Pail    120 lb Keg    400 lb Drum

RLI Product Item #				        88801	88804	           88805	   88806