MaxxLife™ HT 220 High Temperature Multipurpose Grease

NLGI # 2

This High Temperature EP grease is a state-of-the-art product, characterized by exceptional mechanical and oxidation stability.

MaxxLife HT™ 220 is the little brother to the heavy duty MaxxLife HT™ 600 (see MaxxLife HT 600 data sheet). The very high load carrying ability, excellent resistance to water, superior corrosion protection, and outstanding performance in a wide temperature range, make it a high performance premium multipurpose grease. It contains no heavy metals or other harmful or environmentally undesirable additives. This EP grease is formulated with a state-of-the-art overbased calcium sulfonate thickener that gives long life at high temperatures, high extreme pressure characteristics and exceeds NLGI GC/LB (ASTM D-4950).

Applications: Industrial and mining machinery, transportation, agricultural, marine applications, construction and forestry

equipment, paper mills, conveyors, journal bearings, electric motors, and pumps can benefit from its long lasting protection.

- Unique high performance multipurpose automotive and industrial grease

- Increases bearing life 2-4 times over conventional (soap-based) grease lubricants (e.g. Lithium/Lithium Complex, etc.)

- Provides significant protection in automotive, industrial and agricultural wheel bearing applications where temperatures can be high due to heat from disc brakes

- Excellent for chassis lubrication because of superior low temperature properties, shear stability, and water resistant

- Preferred grease for lubrication of antifriction bearings

- Recommended for (Seal For Life) Applications

- Outstanding corrosion protection

- Environmentally friendly

- Excellent compatibility with other greases

Typical Specifications:

Base Oil	Viscosity SUS @ 100 oF 			ASTM- D 445			1100

Viscosity SUS @ 210 oF 							85

V.I. 									95

Pour Point, oF					ASTM- D 97			 +5

Operating Temperature Range 				ASTM- D-566			-20°F to +350°F

Color										Tan

Texture										Buttery

Appearance									Smooth

Dropping Point F oF (oC) 				ASTM- D-	2265			+572 (+300)

Water washout @ 79oC (175oF) % loss 			ASTM- D-	1264			2.75

4-Ball wear test m.m scar, 40kg, 1200 RPM 75oC, 1 H 		ASTM- D-2266			0.39

4-Ball EP test 					ASTM- D-2596

LWI, kg 									65

Weld point, kg 								500

Timken OK load lbs 					ASTM- D-2509			65

Pen. @ 250C (77oF) mm/10				ASTM- D-217

Pen. worked 60 strokes 							270

Pen. worked 10,000 strokes change from 60 strokes 					-1

Pen. worked 100,000 strokes change from 60 strokes 					+2

Roll Stability Pen.					ASTM- D-1831			 +19

Oil Separation -24 hours @ 25oC (77oF)			ASTM- D-	1742			 0.17

Rust test rating 					ASTM- D-	1743			Pass

Oxidation Stability –Pressure Vessel Oxidation		ASTM- D-942

psi press. drop/100 hours 							0

psi press. drop/500 hours 							2

psi press. drop/1000 hours 							9

Salt Fog Corrosion hrs 				ASTM- B-	117			4,000

Wheel bearing leakage grams, modified @ 163oC (325oF) 	ASTM- D-	1263			0.40

LT-37 Mobility 					LT-37

40oF 									133.1 g/minute

0oF 									4.98 g/minute

* Trademark of Renewable Lubricants, Inc.

Copyright 1999 Renewable Lubricants, Inc.

Availability	F.O.B. :Manufacturer	 16 oz. Tube    35 lb  Pail    120 lb Keg    400 lb Drum

RLI Product Item #				          89001	89004	          89005	    89006